Supplementary Material

Multiple-reaction kinetics of composite electrodes for sulfide-based all-solid-state batteries: Impedance decoupling

Siwon Kima, Junhee Kanga, Jae Hyun Parkb, Jong-Won Leea,b,*

a Division of Materials Science and Engineering, Hanyang University, 222 Wangsimni-ro, Seongdong-gu, Seoul 04763, Republic of Korea

b Department of Battery Engineering, Hanyang University, 222 Wangsimni-ro, Seongdong-gu, Seoul 04763, Republic of Korea

* Corresponding author.

E-mail address: jongwonlee@hanyang.ac.kr (J.-W. Lee)

Supplementary Note 1. Analytical solution for impedance of TLMs

The analytical solution of the total impedance of the ion blocking–ion blocking TLM is:

Ztotal=z1z3z1+z3L+2z32z2z1+z332coshLz1+z3z2-1sinhLz1+z3z2,

where z1 and z3 are ionic impedance and electronic impedance per unit surface area, respectively, z2 is interfacial impedance per unit volume, and L is the thickness of the composite electrode.

The ionic or electronic impedance with grain boundary components is given by:

z=rbulk+11rgb+(jω)ηcgb,

where rbulk and rgb are bulk resistance and grain boundary resistance, respectively, and cgb, ω, and η are parameters representing grain boundary CPE.

The analytical solution of the total impedance of the electron blocking–ion blocking TLM is:

Ztotal=z1z3z1+z3L+z2z1+z332z12+z32coshLz1+z3z2+2z1z3sinhLz1+z3z2,

where z1 and z3 are ionic impedance and electronic impedance per unit surface area, respectively, z2 is interfacial impedance per unit volume, and L is the thickness of the composite electrode.

The generalized Finite-length Warburg component is described by the following equation:

zw=rwcoth(jωTw)α(jωTw)α,

where rw is the resistance for the diffusion process in a solid phase of active materials, Tw is the time constant for diffusion, and α is the power-law exponent that accounts for the frequency dispersion.

Table S1. Parameters used in equivalent circuit modeling of the ion blocking–ion blocking condition (Fig. 2).

|  | ri,bulk (Ω cm) | ri,gb (Ω cm) | ci,gb (μF cm−1 sη-1) | re,bulk (Ω cm) | re,gb (Ω cm) | ce,gb (μF cm−1 sη-1) | cint (F cm−3 sη-1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2b | 1000 | - | - | 1000 | - | - | 0.01 |
| 2c (upper) | 500, 1500 | - | - | 1000 | - | - | 0.01 |
| 2c (lower) | 1000 | - | - | 800, 1200 | - | - | 0.01 |
| 2d | 500 | 500 | 0.01 | 1000 | - | - | 0.01 |
| 2e (upper) | 250, 750 | 1000−ri,bulk | 0.01 | 1000 | - | - | 0.01 |
| 2e (lower) | 500 | 500 | 0.001, 0.1 |  |  |  | 0.01 |
| 2f | 1000 | - | - | 500 | 500 | 0.01 | 0.01 |
| 2g (upper) | 1000 | - | - | 250, 750 | 1000−ri,bulk | 0.01 | 0.01 |
| 2g (lower) | 1000 | - | - | 500 | 500 | 0.001, 0.1 | 0.01 |

*Electrode thickness L was fixed to 200 μm.

Table S2. Parameters used in equivalent circuit modeling of the electron blocking–ion blocking condition (Fig. 3).

|  | ri (Ω cm) | rint (Ω cm3) | cint (F cm−3 sη-1) | re (Ω cm) | zw |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | rw (Ω cm3) | Tw (s) |
| 3b | 1000 | - | 0.001 | - | - | - |
| 3c | 1000 | 0.5 | 0.001 | - | - | - |
| 3d | 1000 | 0.5 | 0.001 | - | 1 | 10 |
| 3e | 1000 | 0.5 | 0.001 | 1000 | 1 | 10 |
| 3f | 500, 1500 | 0.5 | 0.001 | - | 1 | 10 |
| 3g | 1000 | 0.3, 0.8 | 0.001 | - | 1 | 10 |

*Electrode thickness L was fixed to 200 μm.

Table S3. Fitting results for symmetric cells (Fig. 4).

|  | L (μm) | Ri,bulk (Ω cm2) | Ri,gb (Ω cm2) | CPEi,gb |  | Re (Ω cm2) | CPEint |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | C (μF cm−2 sη-1) | η (-) |  | C (mF cm−2 sη-1) | η (-) |
| 62 wt% | 190 | 9.3 | 25.6 | 4.8 | 0.69 | 336.8 | 6.3 | 0.78 |
| 72 wt% | 180 | 18.7 | 29.4 | 53.1 | 0.60 | 7.4 | 14.9 | 0.63 |
| 82 wt% | 160 | 12.8 | 6.2 | 262.7 | 0.61 | 3.7 | 18.3 | 0.60 |
| 45 °C | 190 | 8.0 | 12.4 | 5.2 | 0.72 | 256.8 | 7.2 | 0.80 |
| 60 °C | 190 | 6.0 | 3.1 | 5.7 | 0.81 | 181.2 | 9.6 | 0.83 |

Table S4. Fitting results for three-electrode full cells (Fig. 5).

|  | L (μm) | Ri (Ω cm2) | Rint (Ω cm2) | CPEint |  | Re (Ω cm2) | Zw |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | C (μF sη-1) | η (-) |  | Rw (Ω cm2) | Tw (s) | α (-) |
| 62 wt% | 47.5 | 8.7 | 22.4 | 34.5 | 0.97 | 84.2 | 215.5 | 2929.3 | 0.31 |
| 72 wt% | 45 | 12.0 | 18.2 | 27.1 | 0.89 | 1.9 | 40.6 | 614.6 | 0.24 |
| 82 wt% | 40 | 4.7 | 17.2 | 58.8 | 0.80 | 0.9 | 37.2 | 676.0 | 0.30 |
| 45 °C | 47.5 | 5.1 | 8.7 | 64.7 | 0.97 | 64.2 | 106.4 | 1207.5 | 0.36 |
| 60 °C | 47.5 | 2.3 | 7.6 | 53.9 | 0.94 | 45.3 | 81.0 | 2350.0 | 0.27 |

Fig. S1. (a) Impedance spectra of symmetric cells employing VGCF measured at temperatures of 30, 45, and 60 °C and (b) corresponding quantification results. (c) Impedance spectra of full cells employing VGCF measured at temperatures of 30, 45, and 60 °C and (d) corresponding quantification results.

Table S5. Fitting results for symmetric cells employing uncoated NCM811 (Fig. 6a).

|  | L (μm) | Ri,bulk (Ω cm2) | Ri,gb (Ω cm2) | CPEi,gb |  | Re (Ω cm2) | CPEint |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | C (μF sη-1) | η (-) |  | C (mF sη-1) | η (-) |
| 62 wt% | 210 | 12.2 | 50.5 | 4.6 | 0.69 | 127.2 | 1.6 | 0.84 |
| 72 wt% | 230 | 12.9 | 80.3 | 14.2 | 0.65 | 10.4 | 1.1 | 0.87 |
| 82 wt% | 210 | 59.7 | 209.5 | 9.7 | 0.63 | 6.2 | 2.3 | 0.83 |
| 45 °C | 230 | 14.3 | 37.0 | 16.7 | 0.67 | 7.3 | 2.2 | 0.82 |
| 60 °C | 230 | 10.8 | 8.3 | 55.4 | 0.64 | 4.7 | 3.2 | 0.81 |

Table S6. Fitting results for three-electrode full cells employing uncoated NCM811 (Fig. 6c).

|  | L (μm) | Ri (Ω cm2) | Re (Ω cm2) | Rint (Ω cm2) | CPEint |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | C (μF sη-1) | η (-) |
| 62 wt% | 52.5 | 15.7 | 31.8 | 453.4 | 42.8 | 0.90 |
| 72 wt% | 57.5 | 23.3 | 2.6 | 289.9 | 31.0 | 0.91 |
| 82 wt% | 52.5 | 67.3 | 1.5 | 382.4 | 41.6 | 0.93 |
| 45 °C | 57.5 | 12.8 | 1.8 | 139.6 | 27.2 | 0.93 |
| 60 °C | 57.5 | 4.8 | 1.2 | 67.8 | 31.6 | 0.92 |

Table S7. Parameters used in equivalent circuit modeling with varied Rint/Ri values (Fig. 6e).

| Rint/Ri | ri (Ω cm) | rint (Ω cm3) | cint (F cm−3 sη-1) | zw |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | rw (Ω cm3) | Tw (s) |
| 3 | 1000 | 1.2 | 0.001 | 1 | 10 |
| 1 | 2500 | 1 | 0.001 | 1 | 10 |
| 1/4 | 5000 | 0.5 | 0.001 | 1 | 10 |
| 1/16 | 10000 | 0.25 | 0.001 | 1 | 10 |

*Electrode thickness L was fixed to 200 μm.