Supplementary Information

Conflicting Roles of Conductive Additives in Controlling Cathode Performance in All-Solid-State Batteries

Minhyeong Cho, Jonghyeok Yun, Junhee Kang, Siwon Kim, Jong-Won Lee*

a Division of Materials Science and Engineering, Hanyang University, 222 Wangsimni-ro, Seongdong-gu, Seoul 04763, Republic of Korea

* Corresponding author.

E-mail addresses: jongwonlee@hanyang.ac.kr (J.-W. Lee)

Fig. S1. Nyquist plot of the AC-impedance spectrum for LPSCl.

Fig. S2. Nyquist plot of the AC-impedance spectrum for LZC.

Fig. S3. SEM image of VGCF particles.

Fig. S4. N2 adsorption/desorption isotherms of VGCFs.

Fig. S5. SEM images for (a) low- and (b) high-fAM electrodes without CAs.

Table S1. Fitted parameters for the pristine and cycled electrodes.

| Pristine |  | R1 (Ω cm) | Rion (Ω cm2) |  | Rint (Ω cm2) | Rw (Ω cm2) | CPEint |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | C (mF sη−1cm−2) |  | η (−) |
| Low-fAM | w/o CA | 891.1 | 64.8 | 145.0 |  | 22.1 | 0.7 | 0.7 |  |
|  | with CA | 926.0 | 80.9 | 175.2 |  | 18.3 | 1.1 | 0.5 |  |
| High-fAM | w/o CA | 1742.3 | 318.8 | 241.1 |  | 86.7 | 1.4 | 0.4 |  |
|  | with CA | 1747.6 | 402.5 | 278.0 |  | 64.5 | 4.8 | 0.7 |  |

| Cycled |  | R1 (Ω cm) | Rion (Ω cm2) |  | Rint (Ω cm2) | Rw (Ω cm2) | CPEint |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | C (mF sη−1cm−2) |  | η (−) |
| Low-fAM | w/o CA | 1244.8 | 108.2 | 285.1 |  | 28.7 | 0.7 | 0.7 |  |
|  | with CA | 1370.2 | 140.1 | 381.0 |  | 27.6 | 1.2 | 0.4 |  |
| High-fAM | w/o CA | 2227.0 | 416.9 | 490.3 |  | 105.3 | 1.2 | 0.9 |  |
|  | with CA | 2013.5 | 780.9 | 591.4 |  | 41.9 | 3.6 | 0.7 |  |

Table S2. Porosity and tortuosity of composite electrodes.

| Sample |  | Porosity | Tortuosity |
| --- | --- | --- | --- |
| Low-fAM | w/o CA | 0.14 | 6.47 |
|  | with CA | 0.15 | 7.56 |
| High-fAM | w/o CA | 0.18 | 17.41 |
|  | with CA | 0.19 | 18.34 |

Fig. S6. Voltage profiles of ASSBs with low-fAM electrodes (a) without and (b) with CAs during the cycling test at 0.33C.

Fig. S7. Voltage profiles of ASSBs with high-fAM electrodes (a) without and (b) with CAs during the cycling test at 0.33C.

Fig. S8. DC-polarization measurements of high-fAM electrodes with LZC.

Fig. S9. Voltage profiles of high-fAM electrodes using LZC (a) without and (b) with CAs during the cycling test at 0.33C.