Methods (simulation + DFT) — revision v8

DFT · DEM 두 축을 한 문서로 — 공저자 검토용 교체안, 2026-08-30

PROVISIONAL — NOT FOR SUBMISSION

이 문서는 투고용 최종본이 아니라 ① 지금 확정된 문장을 그대로 붙여넣을 수 있게 정리하고 ② 아직 값이 없는 칸을 공란으로 드러내기 위한 것입니다. 공란은 값이 작아서 생략한 것이 아니라 아직 재지 않았다는 뜻입니다.

# 0. 공란이 어디인가 — 먼저 볼 것

본문·표·캡션에서 값이 비어 있는 자리는 아래 넷뿐입니다. 나머지는 전부 확정문입니다.

| 자리 | 무엇이 없나 | 누가 채우나 | 언제 |
| --- | --- | --- | --- |
| Figure 2e · 본문 34 | SDCP vs PTFE 흡착에너지 대비 [ A ] | DFT 계산 | 제출 후 약 4일 |
| Table S1 | 없음 — 파라미터는 전부 확정 | — | 지금 |
| Table S3 σ_ion | 이온 전도도 시뮬 값 | DEM 트랙(별도 브랜치) | 미정 |
| Table S3 Areal capacity | 비용량 (mAh g⁻¹) | 공저자 회신 | 회신 즉시 |

⚠ Figure 2e 의 공란 [ A ] 는 문장 안의 숫자 한 자리입니다. 그 값이 오면 다른 문장은 하나도 바꾸지 않고 그 자리만 채우면 됩니다 — §5 에 들어갈 문장을 미리 적어 두었습니다.

# 1. v6 대비 무엇이 바뀌나 (DFT 축)

| 항목 | v6 | v8 |
| --- | --- | --- |
| 계산 코드 | Quantum ESPRESSO 로 서술 | VASP (PAW) — 인용할 값이 이 트랙의 산출입니다 |
| 기하 | 서술 없음 | UMA 이완 기하 위의 단일점 — DFT 최소점이 아님을 명시 |
| 자기 상태 | "반강자성 (net 0), Ni 1.02 μB" | 시작 배치를 선언하고, 실현된 모멘트를 기록하는 방식으로 서술 |
| 기준계 대칭성 | 서술 없음 | 복합체·슬랩·기체가 모두 같은 스핀 구속 정책 — 이것이 v6 세대 값을 보류시킨 원인 |
| 분산 보정 | "Grimme D3" | D3 zero damping 으로 명시 (D3-BJ 아님) |
| 기전 문장 | 술포네이트가 표면과 상호작용한다 | 삭제 — 계산이 그 기전을 보이지 않습니다 (§6) |

# 2. Methods — DFT · 설명형 (Full)

지면이 허용되면 이쪽을 씁니다. 영문 그대로 붙여넣으면 됩니다.

DFT calculations. Spin-polarised DFT calculations were performed with VASP using projector augmented-wave potentials and the Perdew–Burke–Ernzerhof functional, with Grimme's D3 dispersion correction in the zero-damping form and a rotationally invariant Dudarev +U correction of U − J = 6.2 eV applied to the Ni 3d states. The plane-wave cut-off was 520 eV with an electronic convergence threshold of 1 × 10⁻⁶ eV, Gaussian smearing of 0.05 eV, aspherical gradient corrections within the PAW spheres, and real-space projection disabled.

The NCM811 surface was represented by a LiNiO₂(104) slab (1 × 4, four layers, 192 atoms, 18.27 × 11.51 Å in plane) with more than 15 Å of vacuum, a Γ-centred 3 × 4 × 1 k-mesh, and a dipole correction along the surface normal. SDCP was represented by its sulfonate-functionalised EDOT repeat unit (C₁₁H₁₆O₆S₂) and PTFE by a C₁₀F₂₂ segment; gas-phase references were computed in cubic boxes with 20 and 24 Å of padding, the reference energy changing by 0.3 meV between them.

Adsorption configurations were pre-screened over seven surface sites and 48 molecular orientations with the UMA-s-1p1 machine-learned interatomic potential, relaxing the adsorbate together with the outermost 15 % of the slab. The DFT energies reported here are static single points on those machine-learned geometries and are not DFT local minima; identical fixed geometries and an identical computational protocol were used for every species, so that the comparison is made at matched geometry rather than at matched relaxation.

The magnetic state of the slab was declared rather than optimised. Each calculation started from a collinear antiferromagnetic configuration of the 48 Ni sites (24 up, 24 down, ±1 μB initial moments) with the total moment left unconstrained in the complexes, the clean slab and the gas-phase references alike, so that no species was constrained relative to another. The realised site-projected moments were recorded for every calculation, and energies were differenced only between calculations that realised the same magnetic configuration.

Adsorption energies were obtained as   E_ads = E_slab+adsorbate − E_slab − E_adsorbate.   (1)

Limitations. These are vacuum, 0 K, single-molecule quantities evaluated on fixed, machine-learned geometries. They are not adhesion energies, interfacial resistances or coverage-dependent quantities, and the two adsorbates are molecular segments rather than polymers — a real polymer chain contacts the surface at many points simultaneously. Total energies are code- and pseudopotential-specific and are meaningful only as internal differences within this study. The spectroscopic evidence indicates that the as-synthesised SDCP is self-doped, whereas the adsorption model is the neutral repeat unit; the spin distribution of the doped state is moreover chain-length dependent.

# 3. Methods — DFT · 압축형 (Compact)

같은 사실을 담되 문장 수만 줄인 판입니다. 한정어는 하나도 빼지 않았습니다 — 압축은 문장을 줄이는 것이지 유보를 빼는 것이 아닙니다.

DFT calculations. Spin-polarised DFT calculations were performed with VASP (PAW, PBE) using Grimme D3 dispersion in the zero-damping form, a Dudarev +U correction of U − J = 6.2 eV on the Ni 3d states, a 520 eV cut-off, 1 × 10⁻⁶ eV convergence, 0.05 eV Gaussian smearing and real-space projection disabled. The NCM811 surface was modelled as a LiNiO₂(104) slab (1 × 4, four layers, 192 atoms, 18.27 × 11.51 Å in plane) with more than 15 Å of vacuum, a Γ-centred 3 × 4 × 1 mesh and a dipole correction along the surface normal; SDCP was represented by its sulfonate-functionalised EDOT repeat unit (C₁₁H₁₆O₆S₂) and PTFE by a C₁₀F₂₂ segment, with gas-phase references in 20 and 24 Å boxes (0.3 meV apart).

Adsorption geometries were pre-screened over seven sites and 48 orientations with the UMA-s-1p1 machine-learned potential; the reported DFT energies are static single points on those geometries and are not DFT minima, the same fixed geometry and protocol being used for every species. The slab magnetic state was declared rather than optimised (collinear antiferromagnetic, 24 ↑ / 24 ↓ Ni, ±1 μB initial moments, total moment unconstrained for complexes, clean slab and gas references alike); realised moments were recorded and energies differenced only between calculations that realised the same configuration. Adsorption energies follow E_ads = E_slab+adsorbate − E_slab − E_adsorbate.

These are vacuum, 0 K, single-molecule quantities on fixed machine-learned geometries — not adhesion energies, interfacial resistances or coverage-dependent quantities — and the adsorbates are molecular segments rather than polymers. Total energies are code- and pseudopotential-specific and meaningful only as internal differences. The as-synthesised SDCP is self-doped by the spectroscopic evidence, whereas the adsorption model is the neutral repeat unit.

# 4. Table S1 — 전면 교체 (값은 배포 입력파일 실물)

아래 값은 실제로 배포되는 계산 입력에서 그대로 읽은 것입니다. 공란 없음.

| Category | Parameter | Value |
| --- | --- | --- |
| Method | Code / functional | VASP (PAW); PBE |
|  | Dispersion | Grimme D3, zero damping |
|  | Hubbard correction | Dudarev, U − J = 6.2 eV on Ni 3d |
|  | Plane-wave cut-off | 520 eV |
|  | Electronic convergence | 1 × 10⁻⁶ eV |
|  | Smearing (Gaussian) | 0.05 eV |
|  | Real-space projection | off |
|  | k-point mesh (slab / molecule) | 3 × 4 × 1 / Γ |
| Surface model | Slab | LiNiO₂(104), 1 × 4, four layers, 192 atoms (Li₄₈Ni₄₈O₉₆) |
|  | Cell (in-plane) | 18.27 × 11.51 Å |
|  | Adsorbate–image separation | > 15 Å |
|  | Dipole correction | along surface normal |
| Magnetic state | Starting configuration | collinear AFM, 24 ↑ / 24 ↓ Ni, ±1 μB |
|  | Total-moment constraint | none — for complexes, slab and gas references alike |
|  | Reported | realised site-projected moments per calculation |
| Geometry | Source | UMA-s-1p1 relaxation, outer 15 % of slab free |
|  | DFT treatment | static single point — not a DFT minimum |
| Adsorbate | SDCP repeat unit (neutral) | C₁₁H₁₆O₆S₂ |
|  | PTFE segment | C₁₀F₂₂ |
|  | Gas-phase box padding | 20 and 24 Å (ΔE = 0.3 meV) |
| Search | Potential; sites / orientations | UMA-s-1p1; 7 / 48 |
| Adsorption energy | Definition | Equation (1) |

표에서 빼면 안 되는 세 줄입니다 — 심사에서 반드시 확인하는 항목입니다: 기하가 DFT 최소점이 아니라는 것 · 자기 상태가 선언이라는 것 · 기준계와 복합체가 같은 구속 정책을 쓴다는 것.

# 5. 본문 34 (DFT 문단) — 교체안

아래를 그대로 넣고, 대괄호 한 자리만 나중에 채웁니다.

Density functional theory calculations were used to compare how the two binder chemistries interact with the active material surface (Figure 2e), with the computational model and parameters given in Figure S3 and Table S1. Representative segments of SDCP and of PTFE were placed on a LiNiO₂(104) surface, the adsorption geometry of each being selected by a machine-learned potential over seven surface sites and 48 orientations and then evaluated by DFT at fixed geometry, so that both species are compared under an identical protocol.

[ A ]  Across the four pre-registered poses of each segment, the lowest adsorption energy of the SDCP repeat unit was [ ___ ] eV lower than that of the C₁₀F₂₂ segment.

The calculations describe an isolated repeat unit on a clean, vacuum-terminated surface at 0 K and are therefore a statement about local chemical affinity rather than about adhesion of the processed electrode.

## 삭제해야 하는 문장

v6 원문: "The stronger interaction expected for SDCP originates from its polar sulfonate moieties, which can interact more effectively with exposed surface sites of NCM811 than non-polar PTFE."

→ 삭제합니다. 계산이 그 기전을 보이지 않습니다. 평가된 기하에서 분자와 표면의 실제 최근접 접촉은 탄화수소 C–H 와 표면 O/Ni 사이 2.44 Å 이고, 종전에 근거로 쓰던 술포네이트 O–Li 근접은 재측정에서 4.9–5.4 Å 로 나왔습니다. 술포네이트의 역할은 별도 근거(분광·분산)로 말해야 하며, 흡착 계산이 그것을 뒷받침하지 않습니다.

자리표시자도 함께 삭제: "Additional text related to DFT."

# 6. 캡션 — 교체안

| 위치 | 교체안 (영문) |
| --- | --- |
| Figure 2(e) | Adsorption of representative SDCP and PTFE segments on a LiNiO₂(104) surface, evaluated by DFT at machine-learned geometries. |
| Figure S3 | Computational models used for the DFT calculations: the LiNiO₂(104) slab, the SDCP repeat unit (C₁₁H₁₆O₆S₂) and the C₁₀F₂₂ segment, with the adsorption geometry of each species. |
| Figure 4(a) | DEM-packed and MPM-compacted electronic conduction networks of the SBE and DBE. |
| Figure 4(b) | Effective electronic conductivities of the SBE and DBE under the two binder conventions, each averaged over the eight prescribed grid-origin phases. |

v6 의 "(e) DFT." 와 "Figure S3. DFT" 는 자리표시자입니다.

# 7. 무엇을 주장할 수 있고 무엇은 못 하나

계산이 끝난 뒤에도 아래 구분은 그대로입니다. 미리 정해 둡니다.

| 원고에 쓰려는 문장 | 가능 | 이유 |
| --- | --- | --- |
| SDCP 조각이 PTFE 조각보다 표면에 더 세게 붙는다 | 가능 | 사전등록한 비교량이며 두 조각이 같은 프로토콜입니다 |
| 흡착에너지 절대값 (−0.X eV) | 조건부 | "기계학습 기하 위의 단일점" 을 반드시 함께 적을 때만 |
| SDCP 가 Li 자리를 선호한다 | 불가 | 자리 간 차이가 판정 해상도(30 meV) 아래입니다 |
| 술포네이트가 표면에 앵커링한다 | 불가 | 실제 최근접 접촉이 C–H 이고 기전 근거가 없습니다 |
| 자가도핑 상태의 흡착 | 불가 | 이번 계산은 중성 반복단위만 다룹니다 |
| 전역 최소 자세 / "항상" | 불가 | 자세를 전수로 보지 않았습니다 |

# 8. DEM 축 (Table S2 · S3 · Figure 4)

이 부분은 별도 트랙에서 관리되며, v7 문서의 서술이 그대로 유효합니다. 이 문서에서는 공란 상태만 적어 둡니다.

| 행 | 상태 | 비고 |
| --- | --- | --- |
| σ_ele (두 규약) | 확정 | 본문과 Table S3 에 실을 수 있습니다 |
| 구조 지표 5행 | 확정 | 절대값이 v6 과 다릅니다 — 규약을 함께 적어야 합니다 |
| σ_ion | 공란 | 값이 나왔으나 입력 규약 문제로 사용할 수 없습니다 |
| Areal capacity | 공란 | 비용량(mAh g⁻¹) 회신이 필요합니다 |
| Figure 4(b) | 확정 | 두 규약 병기로 재작도되었습니다 |

# 9. 일정

| 단계 | 소요 | 비고 |
| --- | --- | --- |
| 계산 제출 준비 | 진행 중 | 입력 42건 · 검증 절차 정리 중 |
| 계산 실행 | 약 3–4일 | 동시 실행 10건 이상이면 3일, 8건이면 4일에 가깝습니다 |
| 결과 회수 · 판독 | 1일 | 그 뒤 [ A ] 한 자리를 채우면 §5 가 완성됩니다 |

⚠ 이 문서의 다른 모든 문장은 계산 결과와 무관하게 지금 확정입니다. 기다리는 것은 §5 의 대괄호 한 자리뿐입니다.