Manuscript — Experimental section

Insert after the “Discrete element method” paragraph, replacing the placeholder “Computational details: DFT”. Equations (1) and (2) are already used by the discrete-element section, so the adsorption-energy expression is numbered (3).

Computational details: Spin-polarised density functional theory (DFT) calculations were performed with Quantum ESPRESSO [ref] using the Perdew–Burke–Ernzerhof functional, Grimme D3 dispersion, and a Hubbard correction of U = 6.2 eV on the Ni 3d states. Wave functions and the charge density were expanded to 60 and 480 Ry, respectively, with Gaussian smearing of 0.05 eV and a self-consistency threshold of 1 × 10−6 Ry. The NCM811 surface was modelled as an antiferromagnetic LiNiO2(104) slab (1 × 4, four layers, 192 atoms, 18.27 × 11.51 Å in plane) with more than 15 Å of vacuum, sampled with a Γ-centred 2 × 3 × 1 mesh and a dipole correction along the surface normal. SDCP was represented by its sulfonate-functionalised EDOT repeat unit (C11H16O6S2; the self-doped form C11H15O6S2 was obtained by removing the sulfonate proton) and PTFE by a C10F22 segment. Adsorption configurations were pre-screened over seven surface sites and 48 molecular orientations with a machine-learned interatomic potential [ref], and the lowest-energy configuration of each species on the surface Li and Ni sites was evaluated by DFT. Gas-phase references were relaxed at the Γ point in the same cell until residual forces fell below 1 × 10−3 Ry bohr−1, with the box padding increased from 20 to 24 Å to confirm convergence. Adsorption energies were obtained as

Eads = E(slab+molecule) − E(slab) − E(molecule)(3)

where E(slab+molecule), E(slab), and E(molecule) are the total energies of the adsorbed complex, the clean slab, and the isolated molecule, respectively, all computed with identical settings and the same antiferromagnetic configuration.

Supporting Information

Table S1. Parameters used for the DFT calculations.

| Category | Parameter | Value | Unit | Source |
| --- | --- | --- | --- | --- |
| Method | Program | Quantum ESPRESSO | - | Ref. S1 |
|  | Exchange–correlation functional | PBE | - | Ref. S2 |
|  | Dispersion correction | Grimme D3 | - | Ref. S3 |
|  | Hubbard U (Ni 3d) | 6.2 | eV | Ref. S4 |
| Basis set | Wavefunction cutoff | 60 | Ry | - |
|  | Charge-density cutoff | 480 | Ry | - |
| Brillouin zone | k-point mesh (slab) | 2 × 3 × 1 | - | Γ-centred |
|  | k-point mesh (convergence check) | 3 × 4 × 1 | - | Γ-centred |
|  | k-point mesh (gas-phase molecule) | 1 × 1 × 1 | - | Γ only |
|  | Smearing width (Gaussian) | 0.05 | eV | - |
| Convergence | Total energy | 1 × 10−6 | Ry | - |
|  | Residual force (gas-phase relaxation) | 1 × 10−3 | Ry bohr−1 | - |
| Surface model | Slab | LiNiO2(104), 1 × 4, four layers | - | - |
|  | Number of atoms | 192 (Li48Ni48O96) | - | - |
|  | In-plane dimensions | 18.27 × 11.51 | Å | - |
|  | Cell height | 30.26 | Å | - |
|  | Adsorbate–image separation | > 15 | Å | - |
|  | Constrained atoms | 144 (z ≤ 17.40 Å) | - | - |
|  | Magnetic configuration | Antiferromagnetic (net 0) | - | Ref. S5 |
|  | Ni magnetic moment | 1.02 | μB | Calculated |
|  | Dipole correction | Along surface normal | - | - |
| Adsorbate | SDCP repeat unit (neutral) | C11H16O6S2 | - | - |
|  | SDCP repeat unit (self-doped) | C11H15O6S2 | - | - |
|  | PTFE segment | C10F22 | - | - |
|  | Gas-phase reference box padding | 20 and 24 | Å | - |
| Configuration search | Surface sites / orientations | 7 / 48 | - | - |
|  | Interatomic potential | UMA-s-1p1 | - | Ref. S6 |
|  | Force convergence | 0.05 | eV Å−1 | - |
| Adsorption energy | Definition | Equation (3)a | eV | - |

a Adsorption energies are single-point DFT energies evaluated on the pre-screened adsorption geometries; the adsorbed complexes were not relaxed at the DFT level. The k-point mesh was verified directly for the C10F22 and self-doped SDCP systems; the remaining systems use the same mesh.

Figure captions (DFT panels)

Figure 2e. Calculated adsorption energies of the SDCP repeat unit and a PTFE segment on the LiNiO2(104) surface. ⟨values to be inserted⟩

Figure S3. Computational models used for the DFT calculations: the LiNiO2(104) slab and the adsorbed SDCP (neutral and self-doped) and PTFE segments.

References

[S1] P. Giannozzi, S. Baroni, N. Bonini, M. Calandra, R. Car, C. Cavazzoni, D. Ceresoli, G. L. Chiarotti, M. Cococcioni, I. Dabo, A. Dal Corso, S. de Gironcoli, S. Fabris, G. Fratesi, R. Gebauer, U. Gerstmann, C. Gougoussis, A. Kokalj, M. Lazzeri, L. Martin-Samos, N. Marzari, F. Mauri, R. Mazzarello, S. Paolini, A. Pasquarello, L. Paulatto, C. Sbraccia, S. Scandolo, G. Sclauzero, A. P. Seitsonen, A. Smogunov, P. Umari, R. M. Wentzcovitch, QUANTUM ESPRESSO: a modular and open-source software project for quantum simulations of materials, J. Phys.: Condens. Matter 21 (2009) 395502.

[S2] J. P. Perdew, K. Burke, M. Ernzerhof, Generalized gradient approximation made simple, Phys. Rev. Lett. 77 (1996) 3865–3868.

[S3] S. Grimme, J. Antony, S. Ehrlich, H. Krieg, A consistent and accurate ab initio parametrization of density functional dispersion correction (DFT-D) for the 94 elements H-Pu, J. Chem. Phys. 132 (2010) 154104.

[S4] ── TO BE SUPPLIED: source for U(Ni 3d) = 6.2 eV in LiNiO2.

[S5] ── TO BE SUPPLIED: source for the antiferromagnetic ordering of LiNiO2.

[S6] B. M. Wood, M. Dzamba, X. Fu, M. Gao, M. Shuaibi, L. Barroso-Luque, K. Abdelmaqsoud, V. Gharakhanyan, J. R. Kitchin, D. S. Levine, K. Michel, A. Sriram, T. S. Cohen, A. Das, S. J. Sahoo, A. Rizvi, Z. W. Ulissi, C. L. Zitnick, UMA: A family of universal models for atoms, Adv. Neural Inf. Process. Syst. 38 (2025) 143528–143564.