Comments to the Author(s)

This work examines how LPSC particle size and the CAM/SSE ratio jointly govern ionic/electronic transport and interfacial stability in sulfide all-solid-state composite cathodes, using EIS/DRT, rate-cycling, SEM/FIB-SEM, and a 3D LAMMPS packing simulation. The dataset is systematic and the topic timely; the following points should be addressed before publication:

- The packing simulation omits plastic deformation, which is the central concern. The claim that fine SSE fills voids and lowers porosity/tortuosity rests on a purely Hertzian-elastic, adhesive packing (“elastic contact moduli”) that cannot reproduce the plastic flow it invokes: (i) at 150–300 MPa the LPSC is at or above its yield stress (σ_y ≈ 0.05–0.3 GPa), so the elastic law describes a material that provably yields; (ii) the simulated fine-SSE porosity (19.56%) is about twice the FIB-SEM value (9.43%), because an elastic sphere fills voids only geometrically and saturates near the jamming limit (~20%); (iii) the authors’ own SEM/FIB-SEM (filled interstices, boundary flattening) is plastic morphology, contradicting the model; (iv) NPT densification of elastic, adhesive spheres is reversible (spring-back plus Lennard–Jones clustering), not the irreversible cold-press; (v) elastic point contacts underestimate the conducting neck (A = F/H), inflating the ionic tortuosity. The absolute values (6.360 vs 3.914) thus cannot be compared with experiment, and only the coarse > fine trend is defensible. Please adopt an elastoplastic/hysteretic contact, or present Fig. 2 as a qualitative-trend tool.

- The “molecular-dynamics” framing is inappropriate for micron grains (1 fs, 300 K, and ~0.5 ns total are meaningless for 0.5–6 µm particles): treat it as a granular DEM and show the packing is force-converged. Geometric tortuosity is not transport tortuosity; report the unstated composition, seed count, and scatter. The simulation varies SSE size while every cell varies composition.

- The ionic/electronic trade-off is only half-demonstrated: all data are monotonic (50 > 60 vol%), i.e. only the ion-limited arm, whereas the electron-limited (low-CAM) arm appears only in the simulation. Add a ≤40 vol% NCM90 point showing a U-shaped optimum, or soften “50:50 is optimal” to “50 > 60 within the studied window.”

- The simulated (as-pressed) and FIB-SEM (post-cycling) porosities are different quantities; report the pristine FIB-SEM porosity and state the fabrication pressure separately from the 150 MPa stack. Size and composition are also confounded (coverage vs packing), so degradation is not uniquely from insufficient SSE.

- The DRT-to-CEI assignment is inferential; cross-reference FIB-SEM/XPS and quantify the “hotspots.” Minor: the 50 vol% retention “6.2%” contradicts Fig. 4a and the thesis (likely 96.2%); “long-term cycling” is only 10 cycles; “absence of ion-transport pathways” is too strong (~167 mAh g⁻¹ delivered); Fig. 4c/e use different y-axes; precision (43.11%) lacks error bars; typos remain (#039;, “intrinc”, “LAMPS”).

Overall this is a worthwhile contribution; given the omitted plasticity and the half-demonstrated trade-off, I recommend Major Revision.