Supporting Information –

Integration of DEM-Based Microstructure Generation with FEM and RNM Simulations for Evaluating Ionic Conductivity in Composite Cathodes of All-Solid-State Batteries

Ali Mohammad Bazzoun1,2, Javid Piruzjam1,3, Steffen Hink1, Lukas Rubacek1, Kai Peter Birke2

1Mercedes-Benz AG, Mercedesstraße 120, 70372 Stuttgart, Germany

2Institute for Photovoltaics, University of Stuttgart, Electrical Energy Storage Systems, Pfaffenwaldring 47, 70569 Stuttgart, Germany

3Applied Mathematics, Institute for Modelling and Computational Science, Faculty of Mechanical and Civil Engineering, Helmut Schmidt University/University of the Federal Armed Forces Hamburg, Holstenhofweg 85, Hamburg, 22043, Germany

Figure S1: X-ray Diffraction (XRD) patterns of SE (Li6PS5Cl) and CAM (LiNi0.8Mn0.1Co0.1O2) used in this study.

| Composition [wt.% CAM] | Replicate | Rion, TLM [Ωm-1] | Fit error [%] | Q [Ssαm-1] | α | Rion [Ω] | Cathode 1 thickness [µm] | Cathode 2 thickness [µm] | σioneff [mScm-1] | Electrode area [m2] |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 70 | 1 | 833365 | 1.5 | 19.7 | 0.70 | 282 | 127 | 128 | 0.123 | 0.0000785 |
|  | 2 | 1035415 | 0.26 | 18.7 | 0.67 | 240 | 126 | 129 | 0.135 |  |
|  | 3 | 942202 | 0.97 | 17.0 | 0.68 | 203 | 120 | 124 | 0.153 |  |
| 75 | 1 | 1216000 | 1.7 | 17.8 | 0.74 | 296 | 119 | 126 | 0.105 |  |
|  | 2 | 1254964 | 0.33 | 19.5 | 0.73 | 303 | 119 | 122 | 0.101 |  |
|  | 3 | 1270412 | 0.37 | 19.6 | 0.73 | 317 | 120 | 124 | 0.098 |  |
| 80 | 1 | 1612622 | 0.54 | 17.0 | 0.7 | 392 | 119 | 124 | 0.079 |  |
|  | 2 | 2009708 | 0.29 | 15.1 | 0.71 | 519 | 128 | 131 | 0.063 |  |
|  | 3 | 2345392 | 0.99 | 16.9 | 0.72 | 574 | 122 | 123 | 0.054 |  |

Table S1: Fitted parameters of the Z-type transmission-line model (TLM) and calculated effective ionic conductivity for symmetric composite-cathode cells with varying CAM content (70-80 wt.%), for three replicates each.