2.5. Computational Methods

First-principles density functional theory (DFT) calculations were performed using Quantum ESPRESSO with the Perdew–Burke–Ernzerhof generalized gradient approximation.[1–4] Pseudopotentials from the SSSP efficiency library (ultrasoft for Li, B, P, S, and Cl; projector augmented-wave (PAW) for O) were used with kinetic energy cutoffs of 60 Ry for the wavefunctions and 480 Ry for the charge density.[5–7] The Brillouin zone was sampled with Γ-centered Monkhorst–Pack k-point grids (6 × 6 × 3, 2 × 2 × 1, and 3 × 3 × 1 for LPSC1.6, O-LPSC1.6, and BO-LPSC1.6, respectively),[8] and Marzari–Vanderbilt smearing of 0.01 Ry was applied (0.02 Ry for the structural relaxations of BO-LPSC1.6).[9] Ionic positions were relaxed until all force components fell below 10−3 Ry bohr−1 (10−4 Ry bohr−1 for LPSC1.6), with a self-consistent field (SCF) convergence threshold of 10−8 Ry or tighter.

Three structural models were constructed. LPSC1.6 (Li27P5S22Cl8, i.e., Li5.4PS4.4Cl1.6) was obtained by stacking five primitive argyrodite cells (a ≈ 7.0 Å, α = 60°) along the c axis. Its anion and Li+ disorder was sampled with the Universal Model for Atoms (UMA) machine-learning interatomic potential.[10] The 45 distributions of S2− and Cl− over the free-anion (4a/4d) sites were ranked by UMA energy, Li+ arrangements were sampled for the lowest-energy anion distributions, and the lowest-energy configuration was annealed by UMA-based molecular dynamics (MD) at 500 K for 50 ps. O-LPSC1.6 (Li27P5S21OCl8, i.e., Li5.4PS4.2O0.2Cl1.6) was obtained by replacing one S2− in LPSC1.6 with O2− at the lowest-UMA-energy site among four candidates (one free S2− site and three PS4 corners). BO-LPSC1.6 (Li58P8B2S41O3Cl16, i.e., Li5.8P0.8B0.2S4.1O0.3Cl1.6) was obtained by placing one B2O3 unit (two B3+ on P5+ sites, three O2− on S2− sites, and four added Li+ for charge balance) in a 1 × 1 × 2 LPSC1.6 supercell; the configuration was selected by Ewald pre-screening and UMA relaxation, with the O site confirmed by DFT. Both doped models thus contain the smallest dopant amount each cell allows, more than the experimental samples (0.2 vs 0.045 O and 0.2 vs 0.03 B per formula unit).

For each model, the UMA-optimized cell was isotropically scaled to 0.96–1.06 (LPSC1.6, 11 volumes), 0.94–1.06 (O-LPSC1.6, 7 volumes), or 0.96–1.04 (BO-LPSC1.6, 5 volumes) of its volume, and the ionic positions were relaxed by DFT at each fixed cell. The energy–volume data were fitted to the third-order Birch–Murnaghan equation of state to obtain the equilibrium volume (V0) and bulk modulus (B0),[11] and the ions were finally relaxed at V0; these structures were used in all subsequent analyses. Variable-cell relaxation was not used because a single static configuration of disordered argyrodite does not retain the cubic symmetry of its time-averaged structure.

Li+ transport was simulated by MD with the UMA-s-1p1 model (OMat task) in the Atomic Simulation Environment (ASE).[10,12] The V0 cells (62, 62, and 128 atoms for LPSC1.6, O-LPSC1.6, and BO-LPSC1.6, respectively) were simulated in the NVT ensemble with a Langevin thermostat (time step 2 fs, friction 0.02 in ASE units) at 600, 800, and 1000 K, with 5 ps of equilibration followed by 200 ps of production. At each temperature, three (LPSC1.6 and BO-LPSC1.6) or four (O-LPSC1.6) independent runs with different random seeds were performed. The Li+ diffusion coefficient (D) was obtained from a linear fit of the mean square displacement (MSD), MSD = 6Dt + c, over 2–50 ps with a free intercept c. The activation energy (Ea) was obtained by fitting Eq. (1) to D at the three temperatures, and the ionic conductivity (σ) was estimated from Eq. (2) with a Haven ratio of 1 and D extrapolated to 273 K by Eq. (1), where n is the Li+ number density and q is the Li+ charge.

D=D0exp−EakBT	(1)

σ=nq2DkBT	(2)

Li+ migration pathways were mapped with the bond valence site energy (BVSE) approach on the V0 structures.[13,14] On a grid with ~0.25 Å spacing, the bond valence sum of a Li+ probe was computed over all anions within 5 Å using the softBV parameters (R0 = 2.105, 2.249, and 1.466 Å for Li–S, Li–Cl, and Li–O, respectively; b = 0.37 Å), and the site energy was approximated by Eq. (3), where R is the Li+–anion distance. The Li+ accessible volume fraction was defined as the fraction of grid points within 0.5 (valence units)2 of the global minimum of the periodic map; for display, the maps were resampled into ~9.9 Å near-cubic boxes.

EBV=VLi−12, VLi=XexpR0−Rb	(3)

The density of states (DOS) and projected DOS (PDOS) of BO-LPSC1.6 were calculated non-self-consistently with the optimized tetrahedron method and projections onto atomic orbitals,[15] and were broadened with a 0.05 eV Gaussian for display. Energies were referenced to the valence band maximum (VBM), which was taken from the Kohn–Sham eigenvalues of a fixed-occupation calculation. The electron localization function (ELF) was calculated from the SCF valence density,[16] and its value at the bond midpoint was averaged over all bonds of each type (bonds identified within 2.15, 1.9, 2.3, 2.9, and 2.95 Å for B–S, P–O, P–S, Li–S, and Li–Cl, respectively).

Crystal orbital Hamilton population (COHP) analysis[17] was performed with LOBSTER 5.1.1.[18,19] Because LOBSTER requires PAW wavefunctions, the SCF and non-self-consistent (no symmetry, 960 bands) calculations were repeated on the same structure with PAW datasets from PSlibrary,[7] and the wavefunctions were projected onto the pbeVaspFit2015 basis (Li 1s, 2s, 2p; B and O 2s, 2p; P, S, and Cl 3s, 3p), with a charge spilling of 1.19%. Integrated COHP (ICOHP) values up to the Fermi energy were averaged over each bond type. Bond lengths were averaged over first-shell pairs in the V0 structures (P–S 1.8–2.5, P–O 1.3–1.9, B–S 1.5–2.2, Li–S 1.9–3.2, and Li–Cl 2.0–3.4 Å).

References

1.	P. Giannozzi, S. Baroni, N. Bonini, M. Calandra, R. Car, C. Cavazzoni, D. Ceresoli, G. L. Chiarotti, M. Cococcioni, I. Dabo, A. Dal Corso, S. de Gironcoli, S. Fabris, G. Fratesi, R. Gebauer, U. Gerstmann, C. Gougoussis, A. Kokalj, M. Lazzeri, L. Martin-Samos, N. Marzari, F. Mauri, R. Mazzarello, S. Paolini, A. Pasquarello, L. Paulatto, C. Sbraccia, S. Scandolo, G. Sclauzero, A. P. Seitsonen, A. Smogunov, P. Umari, R. M. Wentzcovitch, J. Phys.: Condens. Matter 2009, 21, 395502.

2.	P. Giannozzi, O. Andreussi, T. Brumme, O. Bunau, M. Buongiorno Nardelli, M. Calandra, R. Car, C. Cavazzoni, D. Ceresoli, M. Cococcioni, N. Colonna, I. Carnimeo, A. Dal Corso, S. de Gironcoli, P. Delugas, R. A. DiStasio Jr., A. Ferretti, A. Floris, G. Fratesi, G. Fugallo, R. Gebauer, U. Gerstmann, F. Giustino, T. Gorni, J. Jia, M. Kawamura, H.-Y. Ko, A. Kokalj, E. Küçükbenli, M. Lazzeri, M. Marsili, N. Marzari, F. Mauri, N. L. Nguyen, H.-V. Nguyen, A. Otero-de-la-Roza, L. Paulatto, S. Poncé, D. Rocca, R. Sabatini, B. Santra, M. Schlipf, A. P. Seitsonen, A. Smogunov, I. Timrov, T. Thonhauser, P. Umari, N. Vast, X. Wu, S. Baroni, J. Phys.: Condens. Matter 2017, 29, 465901.

3.	P. Giannozzi, O. Baseggio, P. Bonfà, D. Brunato, R. Car, I. Carnimeo, C. Cavazzoni, S. de Gironcoli, P. Delugas, F. Ferrari Ruffino, A. Ferretti, N. Marzari, I. Timrov, A. Urru, S. Baroni, J. Chem. Phys. 2020, 152, 154105.

4.	J. P. Perdew, K. Burke, M. Ernzerhof, Phys. Rev. Lett. 1996, 77, 3865–3868.

5.	G. Prandini, A. Marrazzo, I. E. Castelli, N. Mounet, N. Marzari, npj Comput. Mater. 2018, 4, 72.

6.	K. F. Garrity, J. W. Bennett, K. M. Rabe, D. Vanderbilt, Comput. Mater. Sci. 2014, 81, 446–452.

7.	A. Dal Corso, Comput. Mater. Sci. 2014, 95, 337–350.

8.	H. J. Monkhorst, J. D. Pack, Phys. Rev. B 1976, 13, 5188–5192.

9.	N. Marzari, D. Vanderbilt, A. De Vita, M. C. Payne, Phys. Rev. Lett. 1999, 82, 3296–3299.

10.	B. M. Wood, M. Dzamba, X. Fu, M. Gao, M. Shuaibi, L. Barroso-Luque, K. Abdelmaqsoud, V. Gharakhanyan, J. R. Kitchin, D. S. Levine, K. Michel, A. Sriram, T. Cohen, A. Das, A. Rizvi, S. J. Sahoo, Z. W. Ulissi, C. L. Zitnick, arXiv 2025, arXiv:2506.23971.

11.	F. Birch, Phys. Rev. 1947, 71, 809–824.

12.	A. H. Larsen, J. J. Mortensen, J. Blomqvist, I. E. Castelli, R. Christensen, M. Dułak, J. Friis, M. N. Groves, B. Hammer, C. Hargus, E. D. Hermes, P. C. Jennings, P. B. Jensen, J. Kermode, J. R. Kitchin, E. L. Kolsbjerg, J. Kubal, K. Kaasbjerg, S. Lysgaard, J. B. Maronsson, T. Maxson, T. Olsen, L. Pastewka, A. Peterson, C. Rostgaard, J. Schiøtz, O. Schütt, M. Strange, K. S. Thygesen, T. Vegge, L. Vilhelmsen, M. Walter, Z. Zeng, K. W. Jacobsen, J. Phys.: Condens. Matter 2017, 29, 273002.

13.	R. P. Rao, S. Adams, Phys. Status Solidi A 2011, 208, 1804–1807.

14.	H. Chen, S. Adams, IUCrJ 2017, 4, 614–625.

15.	M. Kawamura, Y. Gohda, S. Tsuneyuki, Phys. Rev. B 2014, 89, 094515.

16.	A. D. Becke, K. E. Edgecombe, J. Chem. Phys. 1990, 92, 5397–5403.

17.	R. Dronskowski, P. E. Blöchl, J. Phys. Chem. 1993, 97, 8617–8624.

18.	S. Maintz, V. L. Deringer, A. L. Tchougréeff, R. Dronskowski, J. Comput. Chem. 2016, 37, 1030–1035.

19.	R. Nelson, C. Ertural, J. George, V. L. Deringer, G. Hautier, R. Dronskowski, J. Comput. Chem. 2020, 41, 1931–1940.