# Figure 2e 계산 — 무엇을 왜 재는가

공저자·신규 참여자용 설명서 · 2026-08-30 · v10

이 문서를 읽는 법. 1부만 읽으면 무슨 계산인지, 왜 아직 숫자가 없는지 안다. DFT를 처음 보는 사람 기준으로 썼다. 2부는 원고에 그대로 붙일 영문 문장이다. 3부는 검증 세부라 필요한 사람만 보면 된다.

⚠ 아직 투고용이 아니다. 이 계산은 2026-08-30 현재 한 잡도 돌지 않았다. 2부의 과거형 문장들은 계획된 프로토콜이지 완료된 결과가 아니다.

# 1부 — 배경

## 1-1. 이 계산이 원고 어디에 들어가나

원고의 이야기는 "SDCP라는 바인더를 넣으면 복합 양극이 좋아진다"이다. 그 이야기에는 두 갈래 근거가 있다.

| 갈래 | 무엇을 보이나 | 어디 |
| --- | --- | --- |
| 구조·수송 (DEM/MPM) | SDCP를 넣으면 전자 전도 경로가 촘촘해진다 | Figure 4, Table S3 |
| 분자 수준 (DFT) | SDCP 조각이 활물질 표면과 어떻게 상호작용하나 | Figure 2e, Table S1, 본문 ¶34 |

이 문서는 아래 줄 하나를 다룬다. Figure 2e는 패널 하나이고, 거기 들어갈 숫자를 만드는 것이 전부다.

## 1-2. 흡착에너지란 무엇인가

분자가 표면에 붙는 것이 에너지적으로 유리한지를 재는 양이다. 정의는 뺄셈 하나다.

` E_ads  =  E(표면 + 분자)  −  E(표면)  −  E(분자) `

• E(표면 + 분자) — 분자가 표면에 앉아 있는 계의 전체 에너지

• E(표면) — 분자 없이 표면만

• E(분자) — 표면 없이 분자만, 넓은 빈 상자 안에 (기체 상태)

세 계산이 다 있어야 한 숫자가 나온다. 값이 음수면 붙는 쪽이 유리하다는 뜻이고, 더 음수일수록 더 세게 붙는다.

우리가 답하려는 건 이거다 — SDCP 조각과 PTFE 조각 중 어느 쪽이 더 음수인가.

## 1-3. 왜 이게 오래 걸리나 — 이 계가 까다로운 이유 셋

같은 종류의 계산을 다른 논문들은 몇 주에 끝낸다. 우리가 오래 걸리는 이유는 셋이고, 셋 다 실제로 값을 바꾼다.

### ① 표면이 자석이다

활물질은 니켈이 많은 층상 산화물이다. 니켈은 홀전자를 가져서 자기 모멘트가 있고, 48개 니켈이 위/아래 스핀으로 어떻게 배열되느냐에 따라 계의 에너지가 갈린다. 배열이 다르면 다른 계다.

문제는 뺄셈이다. E(표면+분자)와 E(표면)이 서로 다른 자기 배열로 수렴하면, 뺄셈 결과에 흡착과 무관한 자기 배열 차이가 섞여 들어간다. 이 캠페인이 실제로 그렇게 한 번 물렸다 — 기준계는 자화를 강제로 고정해 놓고 복합체는 자유롭게 풀어서 뺐다. 그건 흡착에너지가 아니다.

그래서 지금은 계산이 끝난 뒤 실제로 어떤 자기 배열로 수렴했는지 읽고, 같은 배열끼리만 뺀다.

### ② 분자를 어디에 어떻게 놓느냐에 따라 값이 달라진다

분자를 표면 위에 놓는 방법은 무한하다. 어느 자리 위에, 어느 각도로, 어느 높이로. 각각을 자세(pose) 라고 부른다.

자세마다 E_ads가 다르다. 그래서 "SDCP의 흡착에너지"라는 단일한 값은 사실 존재하지 않는다. 있는 것은 "우리가 본 자세들 중 최저값" 이다. 이 구분이 이 프로젝트에서 계속 문제가 됐다.

### ③ 셀 설정이 값에 들어간다

DFT 계산은 상자를 무한히 반복해서 푼다(주기 경계). 표면 계산에서는 상자 위쪽에 진공을 충분히 둬서, 분자가 위쪽에 있는 "다음 표면"과 상호작용하지 않게 해야 한다.

⚠ 바로 여기서 이번에 결함이 나왔다 — 1-6에서 다룬다.

## 1-4. 이단 전략 — ML 퍼텐셜로 고르고, DFT로 잰다

자세가 문제라면 자세를 많이 봐야 한다. 그런데 DFT는 비싸다 — 이 계 한 자세가 256코어로 20~45시간이다. 우리가 훑고 싶은 자세는 7자리 × 48배향 = 336개다. 전부 DFT로 돌면 수개월이다.

그래서 두 단계로 나눈다.

| 단계 | 도구 | 무엇 | 비용 |
| --- | --- | --- | --- |
| 1 | UMA-s-1p1 (기계학습 퍼텐셜) | 336자세를 전부 훑고 이완시킨다 | 몇 시간 |
| 2 | VASP (DFT) | 그중 12자세만 골라 정확히 잰다 | 며칠 |

대가가 있다. DFT가 보는 기하는 UMA가 이완시킨 것이지 DFT 자신의 최소점이 아니다. 그래서 우리 값은 엄밀히 말하면 "UMA 기하 위의 고정기하 단일점 에너지" 이고, 원고에 그렇게 적어야 한다. "DFT로 최적화한 흡착에너지"라고 부르면 거짓이다.

용어: 단일점(single point) = 원자를 안 움직이고 그 배치에서 전자 구조만 푸는 계산. 이완(relaxation) = 힘이 0이 될 때까지 원자를 움직이는 계산. 우리는 1단계에서만 이완한다.

## 1-5. 자세를 고른 놈이 답을 정하면 안 된다 — 홀드아웃

여기가 이 프로젝트에서 제일 신경 쓴 부분이다.

UMA가 336자세 중 좋아 보이는 것을 골라 주고, 우리는 그것만 DFT로 잰다. 그런데 UMA가 틀렸으면? UMA가 SDCP 쪽 좋은 자세는 잘 찾고 PTFE 쪽은 못 찾았다면, DFT 결과는 "SDCP가 더 잘 붙는다"고 나오지만 그건 선택기의 편향이지 물리가 아니다.

이걸 시험하려고 자세를 두 묶음으로 나눴다.

| 묶음 | 몇 개 | 어떻게 골랐나 | 역할 |
| --- | --- | --- | --- |
| calibration | 조각당 4 | UMA가 가장 좋다고 한 것들 | 값을 만든다 |
| holdout | 조각당 8 | UMA 점수 사분위별로 2개씩, 표면 접촉 원소가 서로 다르게 | 선택기를 시험한다 |

홀드아웃 8자세는 UMA 점수 전 구간에 걸쳐 있다 — 좋다고 한 것부터 나쁘다고 한 것까지. 그리고 결과를 보기 전에 목록을 동결했다 (해시 3e3ce482…).

시험은 이렇다:

홀드아웃 자세 중 하나라도 calibration 최저보다 30 meV 이상 더 낮게 나오면, UMA의 순위가 틀렸다는 뜻이다. 그러면 그 값을 "더 좋은 자세를 찾았다"고 흡수하지 않고, 선택기 실패로 판정하고 멈춘다.

이게 중요한 이유: 흡수해 버리면 선택기가 틀렸다는 증거가 사라지고, 그냥 더 낮은 숫자만 남는다.

세 갈래로 갈린다.

| 홀드아웃 최저 − calibration 최저 | 판정 |
| --- | --- |
| +30 meV 초과 (홀드아웃이 확실히 높다) | 선택기가 버텼다 → 값을 쓴다 |
| −30 ~ +30 meV (구분 안 됨) | 미해결 — 판정 해상도 안이라 어느 쪽도 말 못 한다 |
| −30 meV 미만 (홀드아웃이 더 낮다) | 선택기 실패 — 값을 쓰지 않는다 |

가운데 칸이 중요하다. 종전 문서는 이 구간을 통과로 처리했는데, 그건 미해결을 성공으로 승격시키는 것이라 틀렸다.

## 1-6. ⚠ 2026-08-30에 발견된 결함 — 진공이 모자랐다

1-3 ③에서 말한 그 문제가 실제로 터졌다.

만들어 둔 자세들의 셀 높이는 30.26 Å이다. 그 안에 4층 슬랩이 들어가고, 남는 위쪽이 진공이다. 그런데 분자가 누워 있는지 서 있는지에 따라 남는 진공이 달라진다.

실측:

|  | 값 |
| --- | --- |
| 검사한 자세 | 24 |
| 진공 15 Å 미만 | 9개 |
| 최악 (PTFE b74) | 8.63 Å — 분자 F가 다음 주기 슬랩 O에서 8.63 Å |

그런데 우리 문서·Methods·Table S1은 전부 ">15 Å" 라고 적고 있었다. 거짓이었다.

왜 안 걸렸나 — 번들 생성기에 진공을 재는 코드가 한 줄도 없었다. 검사는 원자 구성·역할 라벨만 봤다.

8.6 Å이 왜 문제인가: 우리가 쓰는 분산력 보정(D3)은 원자쌍 사이 거리로 계산되는 항이라, 8.6 Å 떨어진 다음 주기 슬랩과도 계속 상호작용한다. 쌍극자 보정(LDIPOL)은 정전기만 다루지 이걸 지우지 못한다.

고친 방법: 셀 높이를 늘려서 모든 자세가 15 Å 이상이 되게 한다. 원자 좌표는 그대로 두고 상자만 키운다.

|  | 이전 | 이후 |
| --- | --- | --- |
| 셀 높이 c | 30.26 Å | 36.66 Å |
| 최소 진공 | 8.63 Å | 15.00 Å |
| 셀 부피 | — | +21 % |

그리고 이제 생성기가 미달이면 번들을 아예 안 만든다. 문장이 아니라 게이트다.

## 1-7. 지금 상태 — 왜 아직 숫자가 없나

|  | 상태 |
| --- | --- |
| 자세 선정 (UMA) | ✅ 끝 — 336자세 훑고 12자세/조각 동결 |
| 계산 묶음 생성 | 🔄 재생성 필요 (진공 결함) |
| VASP 계산 | ⛔ 0잡 — 한 번도 안 돌았다 |
| 값 | ⛔ 없음 |

숫자가 없는 이유는 계산이 어려워서가 아니라 아직 안 돌렸기 때문이다. 돌리면 42잡 · 동시 8개 기준 약 5~6일이다.

## 1-8. 이 계산이 말할 수 없는 것

원고에 쓰기 전에 이 목록을 알아야 한다.

| 못 하는 것 | 왜 |
| --- | --- |
| "SDCP가 PTFE보다 항상 잘 붙는다" | 자세 12개만 봤다. 전역 최소가 아니다 |
| "술폰기가 표면을 붙잡는다" | 자세 집합이 그걸 시험하도록 설계되지 않았다 |
| 실제 전극의 접착력 | 진공·0 K·분자 하나. 접착은 다중 접촉·용매·온도의 문제다 |
| 고분자의 성질 | 우리 모델은 반복단위 하나와 탄소 10개짜리 조각이다 |
| 다른 논문 값과의 직접 비교 | 총에너지는 코드·유사퍼텐셜에 따라 다르다. 내부 차이만 유효하다 |
| 자리 선호 (Li 위 vs Ni 위) | 짝지은 자세가 3개 미만이라 판정 불가 |

# 2부 — 원고에 들어갈 문장

⚠ 삽입 조건: 3부의 게이트가 전부 통과한 뒤에만 넣는다. 그 전까지 아래 과거형은 참이 아니다.

## 2-1. Methods — DFT 절

DFT calculations. Spin-polarised DFT calculations were carried out with VASP using projector augmented-wave potentials and the Perdew–Burke–Ernzerhof functional, with Grimme's D3 dispersion correction in the zero-damping form (IVDW = 11) and a rotationally invariant Dudarev +U correction of U − J = 6.2 eV applied to the Ni 3d states (LMAXMIX = 4). The plane-wave cut-off was 520 eV (PREC = Accurate, ADDGRID = .TRUE.) with an electronic convergence threshold of 1 × 10⁻⁶ eV, Gaussian smearing of 0.05 eV, aspherical gradient corrections within the PAW spheres, real-space projection disabled, and symmetry switched off (ISYM = 0); each calculation was started from superposed atomic charge densities (ISTART = 0, ICHARG = 2). Reported energies are the extrapolated energy(sigma→0) values, not the finite-smearing free energies.

The cathode surface was represented by a stoichiometric LiNiO₂(104) slab used as a proxy for a Ni-rich layered oxide (1 × 4, four layers, 192 atoms, Li₄₈Ni₄₈O₉₆, 18.27 × 11.51 Å in plane, cell height 36.66 Å), with a Γ-centred 3 × 4 × 1 k-mesh and a dipole correction along the surface normal (LDIPOL = .TRUE., IDIPOL = 3). Every adsorbate configuration was constructed so that the shortest distance between the adsorbate and the periodic image of the slab was at least 15 Å. The binder chemistries were represented by a neutral sulfonic-acid-bearing repeat-unit model of SDCP (C₁₁H₁₆O₆S₂) and by a perfluorodecane fragment, CF₃–(CF₂)₈–CF₃ (C₁₀F₂₂). Gas-phase references were single-point calculations on the same fragment conformers used to build the adsorbate configurations, in orthorhombic cells obtained by padding the molecular bounding box (IDIPOL = 4).

Adsorption configurations were pre-screened over seven surface sites and 48 molecular orientations with the UMA-s-1p1 machine-learned interatomic potential, relaxing the adsorbate together with the outermost 15 % of the slab. The DFT energies reported here are static single points on those machine-learned geometries (NSW = 0) and are not DFT local minima. Each selected geometry was held fixed during the DFT single-point calculation, and a common electronic-structure protocol was applied across the compared calculations; the geometries themselves differ between species and between poses, so the reported values include the adsorbate and slab deformation of each pose.

Calibration complexes were initialised from two magnetic seeds — a compensated arrangement of the 48 Ni sites (24 up, 24 down, ±1 μB) and an uncompensated one (26 up, 22 down) — whereas holdout complexes were evaluated only on the prespecified compensated branch. Total magnetisation was unconstrained (NUPDOWN = −1) in the complexes, the clean slab and the gas-phase references alike; the converged local-moment pattern was classified post hoc, and energies were differenced only between calculations that realised the same magnetic configuration.

Adsorption energies were obtained as

E_ads = E_slab+adsorbate − E_slab − E_adsorbate                (1)

Limitations. These are vacuum, 0 K, single-molecule quantities evaluated on fixed, machine-learned geometries at a single coverage; the coverage dependence was not examined. They are not adhesion energies or interfacial resistances, and the two adsorbates are molecular fragments rather than polymers — a real polymer chain contacts the surface at many points simultaneously. Total energies are code- and pseudopotential-specific and are meaningful only as internal differences within this study. The reported comparison is conditional on the compensated magnetic branch and on the finite set of poses examined; it is not a global minimum over adsorption configurations. The spectroscopic evidence indicates that the as-synthesised SDCP is self-doped, whereas the adsorption model is the neutral repeat unit.

## 2-2. 본문 ¶34

⛔ 삭제할 문장 (v6 원문): "The stronger interaction expected for SDCP originates from its polar sulfonate moieties, which can interact more effectively with exposed surface sites of NCM811 than non-polar PTFE." — 근거였던 O···Li 2.09 Å는 2026-08-29 철회됐다 (재측정 4.88–5.39 Å). 자리표시자 "Additional text related to DFT." 도 지운다.

To evaluate a model-level contrast without assigning a functional-group mechanism, we compared a neutral sulfonic-acid-bearing repeat-unit model of SDCP with a perfluorodecane fragment on a stoichiometric LiNiO₂(104) model surface (Figure 2e), with the computational model and parameters given in Figure S3 and Table S1. For each species the adsorption geometry was selected by a machine-learned potential over seven surface sites and 48 orientations, and twelve poses per species — four pre-registered and eight drawn from a stratified prospective holdout — were then evaluated by DFT as static single points at fixed geometry under a common electronic-structure protocol. [숫자 문장] The calculations describe an isolated repeat unit on a clean, vacuum-terminated surface at 0 K, on machine-learned rather than DFT-relaxed geometries, and are therefore a model-level comparison rather than a statement about the adhesion of the processed electrode or about the polymers themselves.

### [숫자 문장] — 방향까지 빈칸이다

결과를 보기 전에 부호를 쓰지 않는다. 빈칸 둘을 채운다.

"Across the twelve poses examined for each species, the lowest adsorption energies of the two models differed by `[___]` eV, the lower value being that of the `[___]`; none of the eight holdout poses fell more than 30 meV below the lowest of the four pre-registered poses."

• 첫 빈칸 = 차이의 절댓값

• 둘째 빈칸 = 그 부호가 정하는 조각 이름 (neutral repeat-unit model 또는 perfluorodecane fragment)

게이트가 막히면 이 문장을 넣지 않는다. 대신:

"Under the pre-registered acceptance criteria the pose-selection assumption was not satisfied, and no pose-resolved energy comparison is quoted (Supporting Information)."

⛔ 붙이면 안 되는 것: "전역 최소" · "가장 안정한 자세" · "적어도 X eV" · "항상" · 자리 선호 · 술포네이트 기전 · binder chemistry · affinity · binding strength.

## 2-3. Table S1 — DFT 파라미터

| Category | Parameter | Value | Unit |
| --- | --- | --- | --- |
| Method | Code | VASP [___] (version) | – |
|  | Functional | PBE (GGA = PE) | – |
|  | Dispersion | Grimme D3, zero damping, IVDW = 11 | – |
|  | Hubbard correction | Dudarev, U − J = 6.2 on Ni 3d; LMAXMIX = 4 | eV |
|  | Plane-wave cut-off | 520 (PREC = Accurate, ADDGRID = .TRUE.) | eV |
|  | Electronic convergence | 1 × 10⁻⁶ | eV |
|  | Smearing / reported energy | Gaussian 0.05; energy(sigma→0) | eV |
|  | Aspherical PAW gradients | on (LASPH = .TRUE.) | – |
|  | Real-space projection | off (LREAL = .FALSE.) | – |
|  | Symmetry / start | ISYM = 0; ISTART = 0, ICHARG = 2; ALGO = Normal | – |
|  | k-point mesh | 3 × 4 × 1 Γ-centred (slab); Γ only (molecule) | – |
| Pseudopotentials | PAW dataset release | [___] | – |
|  | Variants used | Li_sv, Ni_pv, O, C, F, H, S | – |
|  | Provenance | per-job TITEL and SHA-256 in POTCAR_PROVENANCE.json | – |
| Surface model | Slab | stoichiometric LiNiO₂(104) proxy, 1 × 4, four layers, 192 atoms | – |
|  | Cell | 18.27 × 11.51 × 36.66 | Å |
|  | Adsorbate–image separation | ≥ 15.0 (measured minimum 15.00) | Å |
|  | Dipole correction | LDIPOL = .TRUE., IDIPOL = 3 (slab) / 4 (molecule) | – |
| Magnetic state | Calibration seeds | 24 ↑ / 24 ↓ (net 0) and 26 ↑ / 22 ↓ (net +4 μB) | – |
|  | Holdout seed | 24 ↑ / 24 ↓ only | – |
|  | Total-moment constraint | none (NUPDOWN = −1) throughout | – |
|  | Reported | realised local moments, classified post hoc | μB |
| Geometry | Source | UMA-s-1p1 relaxation, outer 15 % of slab free | – |
|  | DFT treatment | static single point, NSW = 0 — not a DFT minimum | – |
| Adsorbate | Neutral repeat-unit model (SDCP) | C₁₁H₁₆O₆S₂ | – |
|  | Perfluorodecane fragment | C₁₀F₂₂, CF₃–(CF₂)₈–CF₃ | – |
|  | Conformer source | same geometry as the adsorbate in the complexes | – |
|  | Gas cell — repeat-unit model | orthorhombic, 32.64 × 29.29 × 29.70 | Å |
|  | Gas cell — perfluorodecane | orthorhombic, 27.26 × 27.25 × 37.87 | Å |
|  | 20 Å vs 24 Å padding — repeat unit | [___] | meV |
|  | 20 Å vs 24 Å padding — perfluorodecane | [___] | meV |
| Configuration search | Potential; sites / orientations | UMA-s-1p1; 7 / 48 | – |
|  | Poses evaluated by DFT, per species | 12 (4 pre-registered + 8 stratified holdout) | – |
| Adsorption energy | Definition | Equation (1) | eV |
| Execution | Jobs / VASP executions | 42 / 43 | – |
|  | Cores per job; site | 256; [___] | – |

## 2-4. 캡션

| 위치 | 교체안 |
| --- | --- |
| Figure 2(e) | "Model-level adsorption comparison: a neutral sulfonic-acid-bearing repeat-unit model of SDCP and a perfluorodecane fragment on a stoichiometric LiNiO₂(104) model surface, evaluated by DFT as static single points on machine-learned geometries. The models are molecular fragments and a proxy surface, not the processed polymers or an explicit NCM811 termination." |
| Figure S3 | "Computational models used for the DFT calculations: the LiNiO₂(104) model slab, the neutral SDCP repeat-unit model (C₁₁H₁₆O₆S₂) and the perfluorodecane fragment (C₁₀F₂₂), with the adsorption geometry of each species." |

Results 에 한 문장 추가 (Figure 2e를 처음 부르는 문장 뒤):

"Both adsorbates are molecular fragments and the surface is a stoichiometric LiNiO₂(104) model rather than an explicit NCM811 termination, so the comparison is model-level."

# 3부 — 검증 세부 (필요한 사람만)

## 3-1. 숫자를 쓰기 전에 통과해야 하는 것

결과를 보기 전에 정해 뒀다. 하나라도 깨지면 숫자를 만들지 않는다.

|  | 게이트 | 왜 |
| --- | --- | --- |
| ① | 조각당 12자세 전부 회수·수렴 | 부분집합에서 최저값을 뽑으면 표본이 줄수록 최저값이 올라간다 |
| ② | 24계산(12자세 × 2조각)이 같은 자기 배열 | 다른 배열끼리 빼면 흡착이 아닌 것이 섞인다 |
| ③ | 홀드아웃 시험 — 1-5의 세 갈래 | 선택기 편향을 시험하는 자리 |
| ④ | 두 조각의 기체 기준이 같은 프로토콜 | 자화 자유·실공간투영 off·같은 상자 관례 |
| ⑤ | 슬랩이 두 조각에 같은 파일 | 해시 일치 |
| ⑥ | 두 자기 시드의 자세별 에너지차 산포 ≤ 10 meV | 시드 민감도가 크면 그 쌍을 막는다 |
| ⑦ | 두 묶음의 VASP·PAW·POTCAR가 동일 | 다른 코드 세대의 값을 합치지 않는다 |
| ⑧ | 이 판정 규약을 사람이 승인 | 현재 proposed — 미승인 |

## 3-2. 계산 묶음

계산은 두 묶음으로 나가고, 두 묶음이 다 회수돼야 한 숫자가 나온다.

|  | calibration 묶음 | holdout 묶음 |
| --- | --- | --- |
| 복합체 | 4자세 × 2시드 × 2조각 = 16 | 8자세 × 1시드 × 2조각 = 16 |
| 기준계 | clean 슬랩 2 + 기체 6 = 8 | clean 슬랩 2 |
| 잡 수 | 24 | 18 |

⚠ 왜 나눴나: 합치면 홀드아웃이 사전등록 후보집합에 섞여서 "결과 보고 고른 것 아니냐"를 막을 수 없다. 나눈 대가는 clean 슬랩 2잡이다.

⚠ 왜 둘 다 필요한가: 기체 기준은 calibration 묶음에만 있고, 12자세는 두 묶음을 합쳐야 나온다. 따라서 두 묶음을 해시로 묶어 함께 분석해야 하고, 그 결합 코드는 아직 없다 — 현재 분석기는 묶음을 하나만 받는다. 이것이 지금 가장 큰 미완이다.

## 3-3. 현재 미완 목록

| # | 무엇 | 상태 |
| --- | --- | --- |
| 1 | 두 묶음 결합 분석 (해시 결속) | ⛔ 미구현 — 이게 없으면 숫자가 나오지 않는다 |
| 2 | 진공 15 Å로 묶음 재생성 | 🔄 생성기는 고쳤다 (게이트 포함), 재생성 필요 |
| 3 | 홀드아웃 시험의 세 갈래 반영 | 🔄 코드가 아직 두 갈래다 |
| 4 | 판정 규약 사람 승인 | ⛔ proposed |
| 5 | POTCAR allowlist·provenance | ⛔ 미해결 |
| 6 | 빈칸 채우기 | ⛔ 계산 후 |

## 3-4. 용어 사전

| 말 | 뜻 |
| --- | --- |
| 슬랩(slab) | 표면을 흉내 내려고 결정을 몇 층만 잘라낸 판 |
| 자세(pose) | 분자를 표면 위에 놓은 한 가지 배치 |
| 단일점(single point) | 원자를 안 움직이고 전자 구조만 푸는 계산 |
| 이완(relaxation) | 힘이 0이 될 때까지 원자를 움직이는 계산 |
| D3 | 원자쌍 거리로 계산하는 분산력(반데르발스) 보정 |
| +U | 니켈 3d 전자의 자기상호작용을 보정하는 항 |
| 시드(seed) | 계산을 시작할 때 넣어 준 초기 자기 배열. 결과가 아니다 |
| 홀드아웃 | 결과 전에 봉인해 둔, 선택기를 시험하기 위한 자세 묶음 |
| 게이트 | 통과 못 하면 값을 만들지 않는 자동 검사 |

## 3-5. 출처

| 무엇 | 어디 |
| --- | --- |
| 게이트·판정 규약 | db/properties/sdcp_stageA_closure_conditions_2026_08_29.json |
| 판정 등재 (미승인) | db/governance/decisions.json |
| calibration 자세 동결 | db/properties/prospective_basins_2026_08_29.json |
| 홀드아웃 자세 동결 | db/properties/prospective_holdout_2026_08_30.json |
| 묶음 생성기 | tools/sdcp/vasp_handoff_bundle.py |
| 이 문서의 모든 수치 | 두 묶음의 MANIFEST.json · INCAR · POSCAR 실측 |