4.5. DFT calculations

DFT calculations were performed with Quantum ESPRESSO [1–3] using the Perdew–Burke–Ernzerhof (PBE) generalized gradient approximation (GGA) [4], with kinetic energy cutoffs of 60 and 480 Ry for the wavefunctions and charge density, respectively. The Brillouin zone was sampled with Γ-centered Monkhorst–Pack k-point grids [5]; the grids, smearing parameters, and convergence thresholds of each calculation are given in the Supplementary Material.

Li migration barriers (Fig. 3f,g) were calculated with the climbing-image nudged elastic band method [6] using seven images, for a Li vacancy hopping between nearest-neighbor Li sites. Li2S was modeled with a 3 × 3 × 3 supercell of antifluorite Li2S (mp-1153 in the Materials Project database [7]) containing a negatively charged Li vacancy compensated by a uniform background charge, and the Li–Nd alloy with a 2 × 2 × 2 supercell of an ordered BiF3-type Li3Nd model (mp-976264) containing a neutral Li vacancy. Ultrasoft pseudopotentials from the GBRV library were used for Li and S [8], and a projector augmented-wave (PAW) dataset from PSlibrary with the Nd 4f electrons frozen in the core was used for Nd [9]. Gaussian smearing was applied to Li2S and Marzari–Vanderbilt smearing [10] to the metallic Li3Nd.

The band gaps of Li2S, Li3P, Li2O, Li3PO4, and LiCl (Fig. 3h) were calculated for structures taken from the Materials Project database [7], with GBRV ultrasoft pseudopotentials for Li, S, and Cl [8] and PSlibrary datasets for P and O [9]. The lattice parameters and atomic positions were fully relaxed, and the band gaps were obtained from the Kohn–Sham eigenvalues at the valence band maximum and conduction band minimum of non-self-consistent calculations with fixed occupations on denser k-point grids.

Interfacial reaction energies between the SEs and NCM (LiNi0.8Co0.1Mn0.1O2) were calculated as a function of voltage (Fig. 5e,f) following the approach of Richards et al. [11], as implemented in pymatgen [12], with the mixed GGA/GGA+U energies of the Materials Project database [7,13]. LPSCl1.6 (Li5.4PS4.4Cl1.6) and NdO-LPSCl1.6 (Li5.44Nd0.02P0.98S4.37O0.03Cl1.6) were represented by the convex-hull energies at their compositions. The interface was treated as open to Li at a chemical potential μLi(φ) = μLi0 − eφ [14], where μLi0 is the chemical potential of Li metal, e is the elementary charge, and φ is the applied voltage vs. Li/Li+ (2.5–4.5 V). At each voltage, the reaction energy was taken as the most negative grand-potential reaction energy over all SE/NCM mixing ratios, normalized per atom excluding Li, and the corresponding reaction products were identified.

The band gaps of the Nd-containing CEI components (Fig. SX) were calculated with the same procedure, but with PAW datasets from PSlibrary for all elements [9], with the Nd 4f electrons frozen in the core.

References

[1]	P. Giannozzi, S. Baroni, N. Bonini, M. Calandra, R. Car, C. Cavazzoni, D. Ceresoli, G. L. Chiarotti, M. Cococcioni, I. Dabo, A. Dal Corso, S. de Gironcoli, S. Fabris, G. Fratesi, R. Gebauer, U. Gerstmann, C. Gougoussis, A. Kokalj, M. Lazzeri, L. Martin-Samos, N. Marzari, F. Mauri, R. Mazzarello, S. Paolini, A. Pasquarello, L. Paulatto, C. Sbraccia, S. Scandolo, G. Sclauzero, A. P. Seitsonen, A. Smogunov, P. Umari, R. M. Wentzcovitch, QUANTUM ESPRESSO: a modular and open-source software project for quantum simulations of materials, J. Phys.: Condens. Matter 21 (2009) 395502. https://doi.org/10.1088/0953-8984/21/39/395502.

[2]	P. Giannozzi, O. Andreussi, T. Brumme, O. Bunau, M. Buongiorno Nardelli, M. Calandra, R. Car, C. Cavazzoni, D. Ceresoli, M. Cococcioni, N. Colonna, I. Carnimeo, A. Dal Corso, S. de Gironcoli, P. Delugas, R. A. DiStasio Jr., A. Ferretti, A. Floris, G. Fratesi, G. Fugallo, R. Gebauer, U. Gerstmann, F. Giustino, T. Gorni, J. Jia, M. Kawamura, H.-Y. Ko, A. Kokalj, E. Küçükbenli, M. Lazzeri, M. Marsili, N. Marzari, F. Mauri, N. L. Nguyen, H.-V. Nguyen, A. Otero-de-la-Roza, L. Paulatto, S. Poncé, D. Rocca, R. Sabatini, B. Santra, M. Schlipf, A. P. Seitsonen, A. Smogunov, I. Timrov, T. Thonhauser, P. Umari, N. Vast, X. Wu, S. Baroni, Advanced capabilities for materials modelling with Quantum ESPRESSO, J. Phys.: Condens. Matter 29 (2017) 465901. https://doi.org/10.1088/1361-648X/aa8f79.

[3]	P. Giannozzi, O. Baseggio, P. Bonfà, D. Brunato, R. Car, I. Carnimeo, C. Cavazzoni, S. de Gironcoli, P. Delugas, F. Ferrari Ruffino, A. Ferretti, N. Marzari, I. Timrov, A. Urru, S. Baroni, Quantum ESPRESSO toward the exascale, J. Chem. Phys. 152 (2020) 154105. https://doi.org/10.1063/5.0005082.

[4]	J. P. Perdew, K. Burke, M. Ernzerhof, Generalized gradient approximation made simple, Phys. Rev. Lett. 77 (1996) 3865–3868. https://doi.org/10.1103/PhysRevLett.77.3865.

[5]	H. J. Monkhorst, J. D. Pack, Special points for Brillouin-zone integrations, Phys. Rev. B 13 (1976) 5188–5192. https://doi.org/10.1103/PhysRevB.13.5188.

[6]	G. Henkelman, B. P. Uberuaga, H. Jónsson, A climbing image nudged elastic band method for finding saddle points and minimum energy paths, J. Chem. Phys. 113 (2000) 9901–9904. https://doi.org/10.1063/1.1329672.

[7]	A. Jain, S. P. Ong, G. Hautier, W. Chen, W. D. Richards, S. Dacek, S. Cholia, D. Gunter, D. Skinner, G. Ceder, K. A. Persson, Commentary: The Materials Project: A materials genome approach to accelerating materials innovation, APL Mater. 1 (2013) 011002. https://doi.org/10.1063/1.4812323.

[8]	K. F. Garrity, J. W. Bennett, K. M. Rabe, D. Vanderbilt, Pseudopotentials for high-throughput DFT calculations, Comput. Mater. Sci. 81 (2014) 446–452. https://doi.org/10.1016/j.commatsci.2013.08.053.

[9]	A. Dal Corso, Pseudopotentials periodic table: From H to Pu, Comput. Mater. Sci. 95 (2014) 337–350. https://doi.org/10.1016/j.commatsci.2014.07.043.

[10]	N. Marzari, D. Vanderbilt, A. De Vita, M. C. Payne, Thermal contraction and disordering of the Al(110) surface, Phys. Rev. Lett. 82 (1999) 3296–3299. https://doi.org/10.1103/PhysRevLett.82.3296.

[11]	W. D. Richards, L. J. Miara, Y. Wang, J. C. Kim, G. Ceder, Interface stability in solid-state batteries, Chem. Mater. 28 (2016) 266–273. https://doi.org/10.1021/acs.chemmater.5b04082.

[12]	S. P. Ong, W. D. Richards, A. Jain, G. Hautier, M. Kocher, S. Cholia, D. Gunter, V. L. Chevrier, K. A. Persson, G. Ceder, Python Materials Genomics (pymatgen): A robust, open-source python library for materials analysis, Comput. Mater. Sci. 68 (2013) 314–319. https://doi.org/10.1016/j.commatsci.2012.10.028.

[13]	A. Jain, G. Hautier, S. P. Ong, C. J. Moore, C. C. Fischer, K. A. Persson, G. Ceder, Formation enthalpies by mixing GGA and GGA+U calculations, Phys. Rev. B 84 (2011) 045115. https://doi.org/10.1103/PhysRevB.84.045115.

[14]	Y. Zhu, X. He, Y. Mo, Origin of outstanding stability in the lithium solid electrolyte materials: Insights from thermodynamic analyses based on first-principles calculations, ACS Appl. Mater. Interfaces 7 (2015) 23685–23693. https://doi.org/10.1021/acsami.5b07517.