Table S2. Computational parameters for the DFT calculations of Li-adatom migration on the Li₃N(001) and LiC₆(0001) surfaces.

| Parameter | Li₃N(001) | LiC₆(0001) |
| --- | --- | --- |
| Code / functional | Quantum ESPRESSO 7.4.1 (pw.x); PBE |  |
| Pseudopotentials | Li, N: ultrasoft | Li: ultrasoft; C: PAW |
| Cutoff (wavefunction / charge density) | 60 / 480 Ry |  |
| k-point mesh | 2 × 2 × 1 (Γ-centred) |  |
| Smearing | Marzari–Vanderbilt, 0.01 Ry |  |
| Convergence (SCF / force) | 1 × 10⁻⁶ Ry / 1 × 10⁻³ Ry bohr⁻¹ |  |
| Slab model | α-Li₃N, 3 × 3; four Li₂N and three Li planes, Li₂N (N-exposed) termination; 135 atoms + 1 Li adatom | Stage-1 LiC₆, √3 × √3 R30°, 2 × 2 × 2; graphene-terminated; 108 atoms + 1 Li adatom |
| Cell / vacuum | a = b = 10.95 Å, c = 28.545 Å, γ = 120°; 15.7 Å vacuum | 15 Å vacuum |
| Fixed atoms | Bottom two Li₂N/Li bilayers | Bottom 50 % of the slab |
| Migration path | Constrained relaxation: adatom lateral (x, y) coordinates fixed; its height and all unconstrained atoms relaxed independently | CI-NEB with the UMA-oc20 machine-learned potential (7 images, IDPP initial path, 0.05 eV Å⁻¹), then DFT single-point energies on those geometries |
| Barrier definition | E(saddle-region configuration) − E(relaxed adsorption minimum) | E(highest-energy image) − E(initial adsorption minimum) |
| Migration barrier | 0.118 eV | 0.290 eV |

Both surfaces use identical electronic-structure settings, so the two barriers are directly comparable. On Li₃N(001) the pronounced adsorbate-induced relaxation of the soft ionic surface destabilised elastic-band calculations, so the barrier was evaluated from two independently converged constrained relaxations instead.

The LiC₆(0001) energies are DFT single points on machine-learned-potential geometries; because such potentials smooth the transition state, the LiC₆ barrier — and hence the barrier ratio quoted in the main text — is a conservative lower bound. The Li₃N(001) value of 0.118 eV agrees with the 0.133 eV reported for the same surface in ref. [54].