Comments on Section 3 (Intrinsic Stability of Sulfide SEs)

Comment 1

Section 3.2 states, on HSAB grounds, that P5+ “belongs to relatively soft Lewis acids” that is attacked by polar solvents. This conflicts with Section 3.1, whose hydrolysis argument requires P5+ to be a hard acid — only then does it prefer the hard base O2− over S2−, driving Li3PS4 + 3H2O → Li3PO4 + 3H2S. If P5+ were genuinely soft, it would retain the soft base S2− and the hydrolysis driving force in Section 3.1 would vanish, so this is not a wording slip but two mechanisms that are mutually inconsistent within HSAB (Pearson groups P5+ with Si4+ and Al3+ as hard acids). Moreover, the donor atoms of NMP (amide N, carbonyl O) are hard bases; under the manuscript’s own “soft P5+”, HSAB would predict a mismatched and therefore weaker attack, so the cited theory does not support the stated conclusion. The nucleophilic-attack mechanism is more consistently described as hard–hard (charge-controlled) substitution at an electron-deficient P center. Whichever classification is adopted, the other section should be reconciled; if both mechanisms coexist, the governing conditions (aqueous versus non-aqueous, charge- versus orbital-controlled) should be stated.

Comment 2

Two chemical descriptions in Section 3.1 would benefit from precision. First, the hydrolysis susceptibility of the soft-base S2− is attributed to a “lowered kinetic barrier,” but HSAB describes a thermodynamic preference, which is distinct from reaction rate; the actual hydrolysis kinetics depend on surface area, crystallinity (amorphous faster than crystalline), and composition. The same thermodynamic/kinetic conflation recurs in the summary sentence (“thermodynamic and kinetic susceptibility”), so the two axes are best separated throughout the section, with the HSAB argument framed as thermodynamic. Second, the P–S bond is called “highly polar covalent,” yet elsewhere the manuscript (including the InF3 passage in Section 3.2) correctly identifies stronger polarizability as the operative property. These are different quantities: with Δχ(P–S) ≈ 0.4 versus Δχ(P–O) ≈ 1.25, the P–S bond is less polar and more covalent than the oxide bond while being more polarizable, and the argument requires high polarizability rather than high polarity. Distinguishing the two terms consistently would remove an internal inconsistency.

Comment 3

Section 3.3 attributes high thermal stability to a “continuous covalent–ionic hybrid bond network,” grouping LGPS, LPSCl, and Li7P3S11 together. Their anion frameworks differ in connectivity: LGPS has (Ge/P)S4 chains, Li7P3S11 contains P2S74− dimers together with PS43−, and LPSCl is fully isolated PS43− plus free S2− and Cl− — the same “structural units” the manuscript itself invokes in Sections 3.1 and 3.2. Describing LPSCl as a continuous network therefore contradicts Section 3.1. Separating the three materials by anion connectivity (isolated, dimer, chain) and linking thermal stability to connectivity would resolve the conflict.

Comment 4

Section 3.3 reports that crystalline sulfides retain their structure to 400–500 °C under inert atmosphere and then concludes that their thermal resistance is “significantly superior to carbonate liquid electrolytes.” The condition and the conclusion are mismatched. Inert-atmosphere decomposition temperature has little bearing on cell-level safety, where the real hazard is the exothermic reaction of the electrolyte with charged cathode active material (lattice-oxygen release) and with lithium metal, whose onset lies well below 400–500 °C. The hazard of carbonate electrolytes, in turn, is governed by flash point, vapor pressure, and thermal runaway rather than decomposition temperature (dimethyl carbonate flash point ≈ 18 °C), so comparing decomposition temperatures compares mismatched axes. The inert-atmosphere qualifier should be carried into the conclusion, and the safety comparison should rest on DSC exothermic onset and heat release (J g−1) under cathode- or lithium-coexisting conditions. Defining a thermal safety margin as (hazard onset − maximum operating temperature) would make the comparison quantitative and remove the possible misreading.

Comment 5

“Bond energy” (and “lattice bond energy”) is used repeatedly as a central explanatory variable — for air stability (Section 3.1), oxysulfide thermal stability (Section 3.3), and the InF3 strategy (Section 3.2) — but is never defined or tied to a measurement. It could denote cohesive energy, bond-dissociation energy, an integrated crystal-orbital overlap population, or a qualitative claim from a cited work. Defining the quantity once, and stating for each cited value whether it was measured or computed under that definition, would make these mechanism arguments verifiable and comparable across sections.

Comment 6

The InF3 passage in Section 3.2 states that the additive “enhances lattice bond energy and reduces polarizability” to preserve conductivity after solvent immersion. Neither phrase appears in the cited work; in that study a lower polarization rate is given as the reason F− substitution lowers ionic conductivity, so the sign is reversed here. The cited work also contains single-dopant controls indicating that In and F act with opposite signs on the conductivity and moisture axes, whereas the solvent-immersion axis actually cited has only pristine-versus-co-doped points. Restating the effect against the paper’s own basis (reduced adsorption energy of H2O and organic solvent), and indicating which element governs which axis, would remove both the reversed causation and the merged attribution.

Comment 7

Section 3.4 contrasts the “true thermodynamic stability range” obtained from first principles with the “apparent” cyclic-voltammetry window. The computed window is itself model-dependent: it shifts with the hull convention adopted for metastable electrolytes (for example, placing an ordered arrangement at Ehull → 0 despite a finite energy), with the configuration chosen, and with the phase set included. Labeling it “true” leads readers to conclude that the experiment is in error. The phrase would be more accurate as “computed (under a given phase set and hull convention),” and the two windows should be described as measuring different quantities — the calculation gives the onset of thermodynamic driving force, the voltammogram the point of measurable current — with the difference attributable to kinetic overpotential and to passivation by decomposition products. The original source of this computational method already provides that explanation, so adding it here carries no additional citation burden.

Comment 8

The three-way interface classification (thermodynamically stable, mixed ionic–electronic conductive, and SEI-like passivated) is useful but could be strengthened in three respects. First, it uses only ionic and electronic transport and omits the mechanical axis, yet Sections 3.5 and 5.1.3 show that volume change and cracking break the interface, so an electronically insulating layer still fails once cracking exposes fresh surface. Second, it provides no observable to distinguish a thermodynamically stable interface from a passivated one — the two appear identical if the impedance does not grow — nor a threshold for what counts as “low electronic conductivity.” Third, it is static, whereas Section 5.1.2’s own “band-gap narrowing leading to electron penetration” implies a passivated-to-mixed-conductor transition over time. Adding a distinguishing observable for each type, an electronic-conductivity or band-gap threshold, a “mechanically retained” condition, and a note that the classification describes an initial state that can evolve, would connect Section 3.4 with Sections 3.5 and 5.1.

Comment 9

Section 3.4 states that an oxide buffer coating “establishes a chemical potential gradient … reducing the driving force for interfacial reactions.” The thermodynamic driving force is set by the chemical potentials of the two end phases and is not reduced by inserting a layer between them. What a coating actually does is to block direct contact, to be self-stable against each side, and to block electron transport; if “gradient” is meant as a stepwise division, then each step can still react, which is precisely the practical difficulty of coating selection. The wording would be more accurate as “blocking direct contact together with self-stability against both sides.” Relatedly, the ideal-coating criteria in Section 4.2.2 (high-voltage stability, ionic conductivity, minimal electronic conductivity, mechanical compliance) consider only the cathode side, but a coating sits between the cathode and the electrolyte and forms two interfaces; adding reactivity against the solid electrolyte as a fifth criterion would substantially strengthen the materials-selection discussion, since in practice reaction with the electrolyte is a harsher screen than reaction with the cathode.

Comment 10

Section 3.4 explains dendrite nucleation and growth through an electronic-pathway mechanism (electronically conductive decomposition products), whereas Section 5.1.1 gives a mechanical “wedge-opening” mechanism (lithium injected at the rear of a crack), explicitly stated to differ from the classical tip-stress model. The relationship between the two — whether they divide nucleation from propagation, or are independent — is not connected. In addition, Section 3.4 names only the electronic conductivity of the decomposition products, whereas Section 5.1.2 also invokes the intrinsic electronic conductivity of the electrolyte itself (recombination of Li+ and e− within the electrolyte). One sentence noting that nucleation proceeds by the electronic path and propagation by mechanics, treated in Section 5.1, and that both the product and the intrinsic electrolyte conductivity contribute, would tie Section 3.4 to Section 5.1.

Comment 11

Three mechanical statements in Section 3.5 rest on quantities of the wrong class or normalization. First, Li2S and Li3P are said to have molar volumes “significantly different from the base phase,” but the per-formula-unit volumes of Li2S (three atoms per unit) and Li6PS5Cl (thirteen atoms per unit) are not directly comparable; a compositional difference is being read as a volume change, and the sign can invert with the normalization basis. The meaningful quantity is the volume change of a balanced reaction, per mole of electrolyte consumed, stating whether the lithium-metal volume consumed at the anode is included, and the sign of “localized volume expansion” is undetermined until the system boundary is drawn. Second, the section sets up “limited fracture toughness” as a cause of degradation, but what is widely reported for sulfides is elastic modulus and hardness, a different class of property from the crack property KIC; low stiffness in fact aids contact conformity, so using modulus as evidence for toughness conflicts with the same section’s formability statement, and a measured KIC (nanoindentation or microbeam) — or a tempered phrasing such as “inferred from reported elastic and hardness data” — would align the property with the claim. Third, the text writes that elastic strain energy “exceeds the fracture toughness threshold,” but strain energy has units of energy while KIC has units of Pa·m1/2; the fracture criterion is G ≥ Gc or K ≥ KIC, and the reference quantity is the energy release rate per new crack area rather than total stored energy, so replacing “fracture toughness” with “critical energy release rate Gc” corrects the statement. The underlying size effect is sound (stored energy scales with d3 and crack energy with d2), so one line deriving the approximately 3 μm threshold and its validity conditions (composition, stack pressure, depth of discharge) would let readers transfer the value.

Comment 12

Section 3.5 states that particle fracture creates “low-impedance pathways” through which lithium penetrates. An empty crack is a pore, so its ionic impedance is in fact effectively infinite; it becomes a low-impedance path only after lithium metal fills it, so the result is being written as a property of the cause. Furthermore, the wedge-opening description in Section 5.1.1 has the opposite order — a crack exists first, and lithium is then injected at its rear — and the manuscript itself notes that this differs from the classical tip-stress model. Rewording to “a mechanically favorable path and a fresh free surface form, which become an electron-conduction path once plated lithium fills them” would make Sections 3.5 and 5.1.1 consistent.

Comment 13

Section 3.5 lists the products of lithium-metal contact as “Li2S, Li3P, and related composite phases,” but the standard grand-potential result for the halide-bearing argyrodite central to this review is Li3P + Li2S + LiCl. The omitted LiCl is the one phase of the three with a wide band gap, and is therefore directly relevant to the low-electronic-conductivity passivation layer targeted in Section 3.4. Adding LiCl connects Sections 3.4 and 3.5.

Comment 14

Several central claims across Sections 3.3–3.5 are stated without conditions or numbers — “significantly” (heat release, cycling improvement), “far exceeds” (voltage), “400–500 °C,” and “1.7–2.1 V.” For the voltage claim in particular, giving both values (layered-oxide operation of roughly 3.0–4.3 V and a sulfide anodic limit of roughly 2.0–2.3 V, noting that the latter is a chemical-potential-referenced computed quantity that must be aligned before being placed beside a cell voltage) would let the reader judge the margin. More generally, comparative claims should carry the number and the condition (method, atmosphere, phase set and hull convention, cycle count and capacity retention) so that they can be transferred to other systems.

Comment 15

The section-closing outlooks — the four “future model requirements” at the end of Section 3.1 and the three “synergistic dimensions” at the end of Section 3.3 — list desiderata without distinguishing what is already partly addressed from what remains open. For example, the “electron–hole coupling” and “solid–gas interface reaction thermodynamics” named in Section 3.1 are partly treated by the manuscript’s own cited references. Appending to each requirement the current state (which reference reaches it) and the remaining gap would turn these outlooks from wish-lists into a roadmap.

Comment 16

A single bond characteristic — the covalent, polarizable P–S bond — is cited with opposite signs across the review: as the weakness in Section 3.1 (low bond energy and high polarizability leading to water attack) and as a strength in Section 3.3 (high decomposition temperature) and Section 3.5 (low modulus and plastic deformation giving good contact). Several remedies likewise improve one axis at another’s expense: oxygen incorporation raises air and thermal stability but lowers ionic conductivity; particle-size reduction aids mechanical stability but worsens air and solvent stability; and polymer compositing raises toughness but dilutes conductivity. Each section’s outlook already flags its own trade-off with a “while maintaining …” clause. Consolidating these into a single cross-axis trade-off table (stability axis against remedy, with the sign on each other axis) would convert scattered caveats into the review’s most useful synthesis, at no additional data cost. As one concrete instance, Section 3.4 requires the interphase to combine high ionic with low electronic conductivity, while Section 3.5 identifies the same product set (notably Li3P) as the driver of volume mismatch and stress; the requirement that a passivation layer be simultaneously electronically insulating and volumetrically compatible is stated nowhere, and one sentence adding it would connect the two sections.

Comment 17

The manuscript already contains every element of the chemo-mechanical feedback loop but never closes it: interface reaction leads to volume mismatch (Section 3.5), then tensile stress (Section 3.5), then cracking and fracture (Section 3.5), which in turn cause passivation breakdown through exposure of fresh surface (Section 3.4), lithium penetration and short circuit (Sections 3.5 and 5.1.1), and disruption of the conduction network (Section 3.5). The only missing arrow is “fresh surface leading to reaction restart.” Drawing this as a single schematic would close the loop and answer directly why degradation accumulates each cycle, as noted by the phrase “during cycling” in Section 3.5. Because it requires only a reorganization of existing content rather than new data, its value relative to cost is high.