## Slide 1
August 2026
Research Seminar
DFT-based screening cascade for sulfide solid electrolytes:
from Li₆PS₅Cl substitution to a 47-dopant funnel
Yonghoon An
Division of Materials Science & Engineering, Hanyang University
(E-mail : yonghoon71@hanyang.ac.kr)
HANYANG UNIVERSITY

## Slide 2
Part 1
1
Why compute? — the screening problem
and why gates matter more than winners
HANYANG UNIVERSITY Battery Materials Lab.

## Slide 3
Motivation
Energy Environ. Sci., 10, 306 (2017).
The screening problem in sulfide solid electrolytes
Composition space grows combinatorially — halogen species, ratio, and dopant are independent knobs.
One experimental point = synthesis + XRD + EIS + cell assembly ≈ weeks. One computed point = hours to days.
Computation does not replace experiment. It decides where the experiment should go.
HANYANG UNIVERSITY
Battery Materials Lab.
3
Approach | Throughput | What it settles
Experiment | weeks / point | ground truth
DFT | hours–days / point | mechanism, absolute energetics
MLIP (surrogate) | minutes / point | ranking, configuration search
→ The cascade exists to spend DFT only where MLIP has already narrowed the field.
Notes: 그림: 왼쪽 조성공간 팬아웃 도식, 오른쪽 47종 funnel 미리보기. Sendek 2017 이 12,000종 스크리닝의 선례.

## Slide 4
Motivation
Screening is only as good as its gates
This talk is not a collection of successes. It also shows the verdicts we retracted.
The value of a screening pipeline is not in picking winners — it is in rejecting wrong candidates.
Every number in this talk carries the protocol that produced it.
HANYANG UNIVERSITY
Battery Materials Lab.
4
Part | Question
1 Motivation | Why compute, and what makes a screen trustworthy?
2 DFT | What does DFT give, and what can it never give?
3 Calculations | Which problem classes have I actually run?
4 Results | Li₆PS₅Cl vs Li₅.₄PS₄.₄Cl₁.₆ — where does the gain come from?
5 Cascade | How does the field screen, and what did we get wrong?
6 Outlook | Atomic scale → particle scale
Notes: 톤 선언 슬라이드. 여기서 청중에게 "실패도 보여준다"를 약속하고 S17 에서 회수한다.

## Slide 5
Part 2
2
Density Functional Theory
— what it gives, and what it cannot
HANYANG UNIVERSITY Battery Materials Lab.

## Slide 6
DFT
HK: Hohenberg–Kohn KS: Kohn–Sham XC: exchange–correlation
The many-electron problem, and the two theorems that solve it
An N-electron wavefunction Ψ(r₁…r_N) lives in 3N dimensions — 100 electrons means 300 dimensions. It cannot be stored.
Hohenberg–Kohn: every ground-state property is fixed by the electron density n(r) alone — three dimensions.
Kohn–Sham: replace the interacting system by a fictitious non-interacting one with the same density.
Everything unknown is pushed into the exchange–correlation functional E_xc[n]. That is the only place approximation enters.
HANYANG UNIVERSITY
Battery Materials Lab.
6
Object | Dimensions | Tractable?
Ψ(r₁…r_N) | 3N | no
n(r) | 3 | yes
KS orbitals ψᵢ(r) | 3 each, N of them | yes
→ DFT is exact in principle. Every practical error traces back to E_xc.
Notes: ⚠ 원전 미보유 — Hohenberg & Kohn (1964), Kohn & Sham (1965) PDF 확보 필요. 발표 전 채울 것.

## Slide 7
DFT
GGA: generalized gradient approx. PBE: Perdew–Burke–Ernzerhof
Energy Environ. Mater., 2 (2019).
Exchange–correlation approximations and what they cost
LDA → GGA (PBE) → meta-GGA → hybrid: accuracy and cost rise together.
Semi-local functionals underestimate the band gap — not "because it is PBE", but because the derivative discontinuity is missing.
DFT+U adds an on-site repulsion to localized d/f states (here: Ni 3d) to offset self-interaction error.
U is an empirical parameter. Always state which atom, which orbital, which value — ours is Ni 3d, U = 6.2 eV.
HANYANG UNIVERSITY
Battery Materials Lab.
7
Notes: Q6 방어: U 를 바꾸면 결과가 바뀐다 → U 를 고정하고 같은 U 안의 차이만 인용.

## Slide 8
DFT
Nature Materials, 18, 1278 (2019).
From total energy to observables — and the boundary
Every property we quote is derived from total energies and their derivatives.
The right column is what we actually judge; the left is what the code returns.
HANYANG UNIVERSITY
Battery Materials Lab.
8
Computed | Derived quantity | What it judges
E(V) curve | BM3 EOS → B₀ | compressive stiffness
finite-strain stress | C_ij → VRH (E, G, B) | elasticity, anisotropy
eigenvalues (fixed-occ nscf) | fundamental gap (VBM–CBM) | electronic insulation
projected wavefunctions | DOS / PDOS | orbital character of band edges
COHP | −ICOHP | bond-resolved strength
grand potential | electrochemical stability window | redox limits
MD trajectory | MSD → D → E_a | ionic transport
⚠ Outside this table: fracture toughness K_IC (a specimen property), μm particle mechanics, quantitative space-charge layers.

## Slide 9
DFT
MLIP: machine-learned interatomic potential NVT: canonical ensemble
Energy Environ. Sci., 13 (2020).
Machine-learned interatomic potentials — why, and how far
DFT scales as O(N³). A 200 ps MD of a 62-atom cell is out of reach.
An MLIP is a regression surrogate for DFT energies and forces — DFT-inherited accuracy at classical-potential speed.
We do not call it "AI computation". It is a surrogate model, not an inference engine.
Limitation that bit us: MLIPs carry no explicit charge state or oxidation state (see Part 5).
HANYANG UNIVERSITY
Battery Materials Lab.
9
Setting | Value
model / task | UMA-s-1p1 / omat
ensemble | Langevin NVT, friction 0.02
timestep / equilibration / production | 2 fs / 5 ps / 200 ps
MSD fitting window | 2–50 ps (fixed by convention)
Arrhenius points | 600 / 800 / 1000 K, multi-seed

## Slide 10
Part 3
3
The calculations I have run
— four problem classes, one protocol
HANYANG UNIVERSITY Battery Materials Lab.

## Slide 11
Methods
BFGS: quasi-Newton optimizer BM3: 3rd-order Birch–Murnaghan
Three-tier pipeline, applied identically to every composition
The same protocol is applied to every composition — otherwise cross-composition comparison is not defined.
HANYANG UNIVERSITY
Battery Materials Lab.
11
Tier 1 MLIP screening | Tier 2 DFT validation | Tier 3 Post-processing
halogen enumeration | MLIP EOS pre-scan | structure: Voronoi, BVSE
Li sublattice screen | BM3 EOS, 11 volumes | electronic: DOS, PDOS, ELF
500 K Langevin anneal | V₀ confirmation (BFGS) | bonding: Bader, ICOHP
→ champion configuration | k-mesh convergence (k×L ≥ 40 Å) | transport: MLIP MD
 |  | mechanics: C_ij (relaxed-ion)
 |  | electrochemistry: ESW

## Slide 12
Methods
Four problem classes — same theory, different setup
Energies from different classes cannot be compared directly. Comparison lives inside a class.
HANYANG UNIVERSITY
Battery Materials Lab.
12
Class | System | Extra variables it introduces
Bulk periodic | Li₆PS₅Cl family | cell type, k-density
Doped supercell | 47 coating dopants | dopant site, concentration, Δe reference
Slab + adsorbate | SDCP × LiNiO₂(104) | vacuum, constraint, coordinate consistency
Isolated molecule | SDCP series (ORCA) | basis set — plane waves are inappropriate
→ Reporting rule: state the class before stating the number.

## Slide 13
Methods
Chem. Mater., 28 (2016). J. Electrochem. Soc., 163 (2016).
What must match before absolute values may be tabulated
Golden rule: if any axis differs, do not build an absolute-value table. Report ranking and direction with a footnote.
HANYANG UNIVERSITY
Battery Materials Lab.
13
Property | Axes that must match | Pseudo-sensitive
Elastic C_ij | pseudo, ecut, k-density, cell type, strain, clamped/relaxed | yes
EOS B₀ | pseudo, ecut, k, composition | yes
Band gap | pseudo, ecut, k, readout method (eigenvalue) | yes
ICOHP | all-PAW required, basis, nbnd | yes (PAW only)
MD (E_a) | MLIP version, MD protocol, multi-seed | no
★ Measured consequence: clamped-ion overstates argyrodite elasticity by ≈2.3× — E_VRH 52.31 (clamped) vs 22.06 GPa (relaxed-ion), experiment ≈23 GPa.
Independent anchor: thiophosphate glass, nanoindentation E ≈ 20 / G ≈ 7 GPa. Our relaxed-ion 22.06 / 8.13 sits there; clamped 52.31 / 20.12 does not.
⚠ Glass vs crystalline argyrodite — this places the value, it does not validate it.

## Slide 14
Part 4
4
Results — Li₆PS₅Cl vs Li₅.₄PS₄.₄Cl₁.₆
and the idea it led to
HANYANG UNIVERSITY Battery Materials Lab.

## Slide 15
Results
f.u.: formula unit
Two argyrodites: same elements, shifted ratio
Per 5 f.u.: Li −3, S −3, Cl +3. Nothing new enters the system.
Reported experimentally: the Cl-rich phase is both faster and stiffer.
Question: where does that gain come from, structurally?
HANYANG UNIVERSITY
Battery Materials Lab.
15
 | Li₆PS₅Cl (LPSCl) | Li₅.₄PS₄.₄Cl₁.₆ (LPSCl₁.₆)
structure | cubic (F-43m) | rhombohedral (R3m)
DFT cell | 52 atoms (4 f.u.) | 62 atoms (5 f.u.)
composition | Li₂₄P₄S₂₀Cl₄ | Li₂₇P₅S₂₂Cl₈
distinguishing defect | — | Li vacancies + 4d-Cl anti-sites

## Slide 16
Results
VBM/CBM: valence-band max / conduction-band min
M1 — the electronic structure is nearly invariant
Fundamental gap 2.066 vs 2.099 eV (Δ = 0.033 eV), from fixed-occupation nscf eigenvalues.
⚠ DOS-threshold readout is not used — it underestimates the gap by ≈0.3 eV.
Band-edge character is also unchanged: VBM is S 3p dominated, CBM is Li 2s + P 3s.
HANYANG UNIVERSITY
Battery Materials Lab.
16
 | LPSCl | LPSCl₁.₆ | message
fundamental gap (eV) | 2.066 | 2.099 | nearly identical
Δ gap (eV) | — | +0.033 | far too small
VBM character | S 3p dominant | S 3p dominant | unchanged
CBM character | Li 2s + P 3s | Li 2s + P 3s | unchanged
→ A >2× difference in transport cannot be explained electronically. The origin must be structural.
Notes: 그림: 두 조성 DOS 겹쳐 그리기. Q1 방어 — 절대 갭이 아니라 같은 방법 안의 차이만 쓴다.

## Slide 17
Results
β: log–log MSD slope (→1 in the diffusive regime)
Energy Environ. Sci., 13 (2020).
M2 — the transport gain has two contributions
E_a (multi-seed, gate-passed): LPSCl₁.₆ = 0.197 ± 0.032 eV.
The Arrhenius prefactor D₀ is larger for the Cl-rich phase — more vacancy carriers.
⛔ LPSCl currently has no citable E_a: the diffusive-regime gate failed 0/6 at 200 ps, and only 1/3 even at 1600 ps.
⛔ We do not quote absolute σ. Reproducibility across groups spans an order of magnitude.
HANYANG UNIVERSITY
Battery Materials Lab.
17
Quantity | LPSCl | LPSCl₁.₆
E_a, multi-seed (eV) | no citable value (gate) | 0.197 ± 0.032
diffusive gate, 200 ps | 0 / 6 pass | pass
diffusive gate, 1600 ps | 1 / 3 pass (1000 K only) | —
Notes: 그림: 아레니우스 플롯 + MSD log-log 에 β 표시. Q2(왜 σ 를 안 보여주나) 의 근거 슬라이드.

## Slide 18
Results
ICOHP: integrated crystal orbital Hamilton population (negative = bonding)
M3 — Li–anion bonding strengthens; the framework does not
The PS₄ covalent framework is unchanged (+1 %). Every Li–anion bond strengthens.
Decomposition of the +13 % average on Li–Cl: a broad vacancy field plus a small number of intense anti-site bonds.
HANYANG UNIVERSITY
Battery Materials Lab.
18
Bond | LPSCl | LPSCl₁.₆ | change
P–S | 5.94 | 6.00 | +1 % (framework intact)
Li–Cl | 1.86 | 2.10 | +13 %
Li–S | 1.59 | 1.72 | +8 %
Li–Cl site type | ¦ICOHP¦ (eV/bond) | bonds | share of the +13 %
LPSCl baseline (all 4a) | 1.855 | 24 | —
LPSCl₁.₆ 4a (vacancy field) | 2.026 (+9.2 %) | 38 (90 % of Cl) | 69 %
LPSCl₁.₆ 4d anti-site | 2.836 (+40 %) | 4 (10 % of Cl) | 31 %
→ Ten percent of the chlorine carries a third of the effect.
Notes: 그림: 결합별 |ICOHP| 막대 (P-S / Li-Cl / Li-S / S-S).

## Slide 19
Results
★ The idea: substitution changes disorder, not electronic structure
M1 — electronic structure invariant. M2 — transport gains from both barrier and carriers. M3 — Li–anion bonds strengthen while PS₄ is untouched.
Taken together: halogen substitution does not rebuild the electronic structure. It creates disorder — Li vacancies and anion anti-sites.
Therefore the screening descriptors should be structural, not electronic.
HANYANG UNIVERSITY
Battery Materials Lab.
19
Observation | Cascade axis it motivates
disorder drives transport (M2, M3) | Li-transport proxy (BVS), disorder promotion (Li–Li std)
framework must survive doping (M3) | structural stability (Δe)
stiffness follows Li–anion bonding (M3) | mechanical axes (E, Pugh ratio)
electronic structure is not the lever (M1) | electronic insulation kept only as a guard, not a target
Notes: 이 슬라이드가 Part 4 와 Part 5 를 잇는 척추. cascade 축 선택의 근거.

## Slide 20
Part 5
5
The cascade — how the field screens,
and what we got wrong
HANYANG UNIVERSITY Battery Materials Lab.

## Slide 21
Cascade
Energy Environ. Sci., 10 (2017). Chem. Mater., 28 (2016).
How the field screens
All three share one shape: start broad, narrow at each step with a physical gate.
Common weakness: the failure rate of each gate is rarely reported.
HANYANG UNIVERSITY
Battery Materials Lab.
21
Work | Entry pool | Filter | Output
Sendek 2017 | ~12,000 Li compounds | ML classifier on cheap descriptors | small candidate set
Xiao 2019 | MP oxide/coating space | thermodynamic filters vs cathode | coating candidates
Richards 2016 | SE × electrode pairs | pseudo-binary interfacial reaction energy | interface stability map
→ Our cascade follows the same funnel, and adds an explicit record of what each gate rejected.

## Slide 22
Cascade
Our cascade: 47 dopants across 14 design axes
Any subset of axes can be combined by geometric mean — one axis at the floor pulls the whole score down (an AND).
⚠ Missing data is not bad data. A candidate lacking a selected axis is excluded from the ranking and reported, never scored as zero.
HANYANG UNIVERSITY
Battery Materials Lab.
22
Group | Axes
electrochemical | oxidative stability, reduction stability, electronic insulation
transport | Li-transport proxy, disorder promotion, dose robustness
mechanical | low stiffness, ductility (Pugh), structural stability (Δe)
practical | lightweight, low cost
air / moisture | qualitative protection tier + literature ΔG_hyd (external, cited)
⚠ Only two of the 47 (Nd₂O₃, B₂O₃) have DFT validation. The rest are MLIP-relative rankings — stated as such wherever they appear.

## Slide 23
Cascade
★ What we got wrong — five retracted verdicts
Each row is a claim we made, then withdrew, and the gate that caught it.
HANYANG UNIVERSITY
Battery Materials Lab.
23
Retracted claim | What was wrong | Gate that caught it
σ ratio 1.33× | single seed | multi-seed requirement
LPSCl E_a = 0.253 eV | MSD never reached the diffusive regime | β gate (0/6 failed)
band gap from DOS threshold | underestimates by ≈0.3 eV | fixed-occupation eigenvalue convention
qualitative air-stability tier | the driver is oxophilicity, not HSAB softness | literature cross-check: 9 of 35 mismatched, all underrated
SDCP E_ads = −0.26 eV | the slab was frozen, so surface relaxation was forbidden | constraint-release control: −1.47 eV, 4× deeper
★ And the −1.47 eV was not adsorption either — structural inspection showed two surface Li⁺ pulled out and coordinated to the sulfonate at 1.91–2.05 Å.
One constraint changed the energy by 4× and changed the physics entirely. Computational design decides the conclusion.
Notes: 이 발표의 차별점. 마지막 줄이 2026-08-06 실측이고 가장 강하다.

## Slide 24
Cascade
Angew. Chem. Int. Ed., 59, 17472 (2020).
Validation strategy — what actually filters
Diffusive-regime gate: β = d log⟨r²⟩/d log t must lie in [0.8, 1.2]. Without it, a caged slope is mistaken for D.
Multi-seed: judgement is made on the β of the ensemble-averaged MSD, not on the mean of per-seed β values.
Literature cross-check: our qualitative air axis against a full transcription of the Zhu 2020 SI, matched by oxidation state.
Structural inspection: a deeper energy is not a bond. Check molecular integrity, contact distance, and atom ejection.
HANYANG UNIVERSITY
Battery Materials Lab.
24
Cross-check outcome | Count
agrees with literature ΔG_hyd | 26
disagrees — all in the same direction (we underrated) | 9
no literature counterpart at matching oxidation state | 12
→ We report what we cannot do: K_IC, μm particle mechanics, quantitative space-charge layers.

## Slide 25
Part 6
6
Conclusions and outlook
HANYANG UNIVERSITY Battery Materials Lab.

## Slide 26
Conclusions
What this work establishes
The Cl-rich gain is structural, not electronic: Li vacancies plus 4d-Cl anti-sites, with 10 % of the Cl carrying a third of the bonding effect.
That finding set the cascade axes — structural descriptors first, electronic ones only as guards.
The gates work. They forced us to retract five of our own verdicts.
Cross-checking against transcribed literature exposed a systematic bias in our qualitative air-stability axis: 9 of 35 wrong, all in one direction.
HANYANG UNIVERSITY
Battery Materials Lab.
26
The contribution is not a winning dopant. It is a pipeline whose failures are visible.

## Slide 27
Outlook
Future plan
Near term: enlarge the LPSCl cell so the diffusive gate can pass; six-point Arrhenius (500–1000 K); SDCP Phase-B in DFT+U.
Mid term: compute ΔG_hyd directly and replace the qualitative air tier; bridge chemistry to mechanics via ΔV_rxn × C_ij.
Long term: hand material constants (E, G, γ, ΔV) to particle-scale DEM, which returns contact area, tortuosity, and effective conductivity.
HANYANG UNIVERSITY
Battery Materials Lab.
27
Scale | Method | What it produces | Status
Å | DFT (+U) | E_xc-level energetics, C_ij, gaps, ESW | established
nm | MLIP MD | D, E_a, configuration search | established, gated
μm | DEM | contact area, tortuosity, effective σ | next
mm | continuum / cell | rate capability, stack pressure window | downstream
Notes: 그림: Å → nm → μm → mm 스케일 사다리에 DFT / MLIP / DEM / continuum 배치.

## Slide 28
Part A
A
Appendix — terminology, settings,
and anticipated questions
HANYANG UNIVERSITY Battery Materials Lab.

## Slide 29
Appendix A1
DFT terminology
Terms are given in the form used in the literature; our internal shorthand is not used on slides.
HANYANG UNIVERSITY
Battery Materials Lab.
29
Term | Meaning | Caution
SCF | self-consistent field — the electron-density iteration | convergence threshold must be stated
pseudopotential | frozen-core replacement of the nuclear potential | USPP / PAW are not interchangeable
k-mesh | Brillouin-zone sampling grid | report k×L, not the grid alone
XC functional | the only approximated term in Kohn–Sham DFT | LDA/GGA/meta-GGA/hybrid differ in cost and bias
DFT+U | on-site Coulomb correction for localized d/f states | empirical; state atom, orbital, and value
smearing (degauss) | fractional occupations near E_F | large smearing biases forces

## Slide 30
Appendix A2
Property terminology
Each entry names the quantity, then the trap that most often breaks its interpretation.
HANYANG UNIVERSITY
Battery Materials Lab.
30
Term | Meaning | Caution
BM3 EOS → B₀ | bulk modulus from an E(V) fit | different quantity from B_VRH — do not mix
C_ij → VRH | polycrystalline average of elastic constants | clamped-ion vs relaxed-ion differ by ≈2.3× here
−ICOHP | bond-resolved bonding strength | ICOHP is negative when bonding; quote magnitudes
ELF | electron localization function, 0–1 | dimensionless; state the isosurface value
Bader charge | charge from a topological partition | partition-dependent; compare within one method
ESW | stability window from a grand-potential diagram | depends on the phase set and hull convention
Pugh ratio B/G | ductility heuristic (>1.75 ductile) | a metals heuristic; argyrodite softness is powder compaction

## Slide 31
Appendix A3
Nature Materials, 18, 1278 (2019).
Transport terminology — the most contested column
This is where a screening talk is most often challenged. Every term below carries its own caveat.
HANYANG UNIVERSITY
Battery Materials Lab.
31
Term | Meaning | Caution
MSD | mean squared displacement ⟨r²(t)⟩ | the fitting window must be stated
β | log–log MSD slope | β→1 defines the diffusive regime; β<0.8 means D is undefined
E_a | Arrhenius activation energy from D(T) | state temperatures, window, and seed count
σ_NE | Nernst–Einstein conductivity, Haven ratio = 1 | an approximation; argyrodite hopping is correlated
D₀ | prefactor z n a₀² ν₀ exp(ΔS_m/k_B) | a softer lattice lowers E_a but also lowers ν₀ and ΔS_m
⛔ We do not quote absolute σ, and we quote ratios only when they pass the multi-seed gate.

## Slide 32
Appendix A4
Computational settings
Reported so that any number in this talk can be traced to the run that produced it.
HANYANG UNIVERSITY
Battery Materials Lab.
32
Task | Code / model | Key settings
Elastic C_ij | QE pw.x | relaxed-ion, 12 strain SCFs (6 Voigt × ±), strain 0.005
EOS B₀ | QE + BM3 fit | 11 volumes, V/V₀ 0.96–1.06
Band gap | QE nscf | fixed occupations, eigenvalue readout
ICOHP | LOBSTER | all-PAW required, extended basis
MD | UMA-s-1p1 (omat) | Langevin NVT, 2 fs, 5 ps eq / 200 ps prod, multi-seed
Slab relaxation | QE + DFT+U | Ni 3d U = 6.2 eV, U-ramp from U = 0, AFM in-plane
⚠ Cross-composition absolute tables are built only when every axis above matches. Otherwise: ranking plus footnote.

## Slide 33
Appendix A5
Anticipated questions (1/2)
HANYANG UNIVERSITY
Battery Materials Lab.
33
Question | Answer
DFT underestimates gaps — why trust 2.07 eV? | We do not use the absolute value. We use the difference within one method (0.033 eV), and the conclusion is that the difference is small.
Why is σ not shown? | Cross-group reproducibility spans an order of magnitude. We retracted our own single-seed 1.33× claim. Ratios are quoted only after the multi-seed gate.
Does MLIP replace DFT? | No. It is a surrogate for the screening stage; champions are re-scored in DFT. MLIPs also carry no explicit charge state, which affected us directly.
Are the 47 dopants experimentally verified? | No. Only two have DFT validation. The rest are MLIP-relative rankings and are labelled as such.
How method-dependent is the ranking? | Strongly. Gate-failing candidates are flattened so gate status and metric value can never cross, and ties are declared meaningless.

## Slide 34
Appendix A5
Anticipated questions (2/2)
HANYANG UNIVERSITY
Battery Materials Lab.
34
Question | Answer
Why U = 6.2 eV? | It is the established value in this lineage and it is empirical. We fix U and quote only differences taken at the same U.
Is Γ-only k sampling acceptable for adsorption? | It propagates into individual E_ads and is footnoted there. The conclusion is the doped–neutral difference, where cell and k are identical and the error largely cancels.
Why is fracture toughness not treated? | K_IC depends on density, grain size and porosity — it is a specimen property, not an atomistic output. We supply elastic constants; above that is DEM and continuum.
Why not tabulate literature ΔG_hyd with your own values? | Different level of theory (MP GGA-PBE plus JANAF experiment, 300 K, specified partial pressures). Mixing external and internal values makes both unusable.
If a constraint changed your result, what about the rest? | Exactly the concern. Constraints are reported with results, and important verdicts are re-run with the constraint released. This talk shows one such case.

## Slide 35
Appendix A6
References held locally
Every citation in this talk corresponds to a PDF and a digest in our literature database.
HANYANG UNIVERSITY
Battery Materials Lab.
35
Topic | Reference
SSE fundamentals, transport, mechanics | Famprikis et al., Nature Materials 18, 1278 (2019)
ML screening of Li conductors | Sendek et al., Energy Environ. Sci. 10, 306 (2017)
High-throughput AIMD screening | Kahle et al., Energy Environ. Sci. 13 (2020)
Interface stability, pseudo-binary | Richards et al., Chem. Mater. 28 (2016)
Electrochemical window, grand potential | Zhu et al. (grand-potential ESW lineage)
Air stability design principles | Zhu & Mo, Angew. Chem. Int. Ed. 59, 17472 (2020)
Elastic properties of superionic conductors | Deng et al., J. Electrochem. Soc. 163 (2016)
Cathode coating screening | Xiao et al. (coating screening)
DFT for battery materials | He et al., Energy Environ. Mater. 2 (2019)
Equation of state | Birch, Phys. Rev. 71, 809 (1947)