## Slide 1
August 2026
Research Seminar
Particle-Resolved Simulation of All-Solid-State Cathodes:
From Powder Packing to Cycle Life
Yonghoon An
Division of Materials Science & Engineering, Hanyang University
(E-mail : yonghoon71@hanyang.ac.kr)
HANYANG UNIVERSITY · Battery Materials Lab.
Notes: 직전 발표(2026-04)는 DEM + DFT 에서 끝났습니다. 오늘은 그 뒤 4개월에 붙은 것 — 소성 압밀, 3D 전도, 전기화학, 사이클 열화, ML — 을 결과 중심으로 보고합니다.

## Slide 2
Introduction
J. Electrochem. Soc. 168 (2021) 040537 · Sci. Rep. 3 (2013) 2261
Battery Materials Lab.
1
■ In an all-solid-state cathode, performance is decided by microstructure
· In a liquid cell the electrolyte soaks every particle. In a solid cell, Li+ passes only where powders were pressed into contact.
· Cathode = active material (AM, NCM811) + solid electrolyte (SE, Li6PS5Cl) powders, cold-pressed at 300 MPa.
· ⇒ What decides performance is not the chemical formula but the microstructure — porosity, where particles touch, and how ions/electrons flow through those contacts.
[Fig] liquid cell (fully wetted) vs solid cell (contact points only)
★ 이 덱에서 가장 중요한 그림 — 새로 그려야 함
[Fig] cold-pressed composite cathode
cross-section (SEM)
Same composition, different pressing → different performance. To see "how", we must look inside.
Notes: 여기서 청중이 잡아야 할 것 하나: 고체에서는 눌러 붙인 자리만 이온이 지나간다. 그래서 미세구조가 전부입니다.

## Slide 3
Introduction
Minnmann et al., J. Electrochem. Soc. 168 (2021) 040537
Battery Materials Lab.
2
■ Experiments cannot see inside — so we rebuild the electrode in a computer
Experiment | What it gives | What it CANNOT give
SEM / EDS | shape of one cut cross-section | 3-D connectivity; where current actually flows
EIS (impedance) | one number for total cell resistance | which contact that resistance comes from
Charge–discharge | the sum of capacity and polarization | which particles are left out, and why
· Input = design numbers (composition · particle size · pressure · thickness · additive wt%).
· Output = what experiments cannot give: contact network · conduction paths · reaction distribution · stress field · cycle degradation.
· This talk reports what that pipeline found — it is not a tool introduction.
Notes: EIS 는 저항을 하나의 숫자로 줍니다. 그 숫자가 어느 접촉에서 왔는지는 못 줍니다. 그걸 나누는 게 이 파이프라인이 하는 일입니다.

## Slide 4
Introduction
Cundall & Strack, Géotechnique 29 (1979) 47 · Sulsky et al., CMAME 118 (1994) 179
Battery Materials Lab.
3
■ Two simulation methods, because compaction is two things at once
 | What happens physically | Method | One-line definition
① | particles roll and settle (rearrangement · stacking · contact) | DEM (discrete element) | treat each particle as a rigid sphere; solve Newton’s equations
② | particles are squashed (plastic deformation · void filling) | MPM (material point) | treat the material as a continuum; solve the deformation
· What DEM cannot do: the sphere never deforms → no shape change.
· What MPM cannot do: a continuum has no "particles" → cannot express "they touched at a point".
· ⇒ Both are required. Either one alone is half the physics.
Notes: DEM 과 MPM 을 처음 듣는 분을 위한 슬라이드입니다. 핵심은 "둘 중 뭐가 낫냐"가 아니라 "둘이 서로 다른 절반을 담당한다"입니다.

## Slide 5
Introduction
Minnmann et al., JES 168 (2021) 040537 (calibration anchor)
Battery Materials Lab.
4
■ The rule that makes it science: never fit one model to the other
· Fitting A to B and then reporting "A and B agree" is circular reasoning.
· Instead each model is calibrated only to experiment, then compared on the quantities they share.
✗ Cross-fitting DEM ⇄ MPM tuned to each other
→ agreement proves nothing
✓ Independent calibration each → experiment, then compare
agreement = cross-validation
· There is exactly ONE calibration point: porosity of pure SE pressed at 300 MPa ≈ 10 % (measured).
· Everything after that is a prediction — composite porosity, thickness, coverage, Heckel yield pressure, absolute σ.
· Agreement = cross-validation. Disagreement = a quantified model limit — information, not failure.
Notes: 질문 1순위가 "결국 실험에 맞춘 거 아니냐"입니다. 답: 보정점은 딱 하나이고, 그 뒤는 전부 예측입니다. 그리고 두 모델은 서로를 절대 안 맞춥니다.

## Slide 6
Introduction
Battery Materials Lab.
5
■ Scope: one cathode layer resolved; the rest are exact boundary conditions
Region | How it is treated
Cathode composite | RESOLVED — every particle, every voxel (9 phases: AM_S · AM_P · SE · VGCF · SuperP · SDCP · SWCNT · PTFE · pore)
Separator | boundary condition (surface supplying Li⁺)
Current collector | one series resistance (bare-Al 46 · C-SUS 30 Ω·cm²)
Li metal anode | reference electrode only → vs-Li half-cell convention
· ★ Why this is not an approximation: in a liquid cell you must solve concentration polarization in the electrolyte. In a single-ion conductor (t⁺ ≈ 1) the anions do not move at all — that term does not exist. It is not omitted; it is absent.
· Pipeline: packing (DEM) → compaction (MPM) → transport (voxel network) → electrochemistry → degradation
Notes: "반쪽셀인데 왜?"라는 질문에 대한 선제 답입니다. 단일이온 전도체에서는 농도 분극 항이 물리적으로 존재하지 않습니다.

## Slide 7
Results and discussion
Minnmann et al., JES 168 (2021) 040537
Battery Materials Lab.
6
■ Two models that never saw each other agree within 1.1 %p — that gap IS the error bar
· DEM (rigid spheres, E_eff 1.35 GPa) and MPM (continuum J2, E 1.53 GPa · ν 0.49 · σ_y 0.30 GPa) were each calibrated only to the same single experiment.
 | MPM | DEM (LIGGGHTS) | Δ
Porosity | 15.93 % | 15.6 % | +0.33 %p
Thickness | 29.95 µm | 30.28 µm | −0.33 µm
Coverage AM_P / AM_S | 49.6 / 48.2 % | 48.3 / 51.8 % | ± 2 %p
Grid convergence 384 → 512: porosity 16.7 → 16.80 % jamming position wall_z 0.616 at BOTH ⇒ the remaining gap is a converged constitutive
difference, not a numerical artifact
[Fig] MPM x–z section (AM + SE + void)
[Fig] porosity vs grid (384 / 512)
To "how much do you trust this simulation?" we can answer with a number: ± 1 %p.
Notes: 이 슬라이드가 이 발표의 신뢰 기반입니다. 서로 본 적 없는 두 모델이 만났고, 격자를 조여도 안 변합니다.

## Slide 8
Results and discussion
Furnas, Ind. Eng. Chem. 23 (1931) · experiment: this lab
Battery Materials Lab.
7
■ Which model owns which observable — proven by a material sweep, not assumed
· Bimodal packing dip = mixing large and small particles has a porosity minimum (small particles fill the gaps between large ones). DEM reproduces it — and matches experiment.
Chart: Porosity vs large:small AM ratio (AM:SE = 80:20)
| S only | 3:7 | 5:5 | 7:3 | P only
DEM (SE D1) | 18.9 | 15.8 | 15 | 14.3 | 16.2
DEM (SE D3) | 20.9 | 17.2 | 15.9 | 14.4 | 16.2
Experiment | 23.9 | 21.3 | 20.3 | 19.8 | 25.4
· MPM gives a monotonic curve (AM 60→95 wt%: 11.7 → 24.5 %) — no dip at all.
· ★ Swept the whole SE material space: soft → monotonic and denser; rigid (E = 24 GPa) → a shallow, mislocated dip but 2–3× too porous (32–48 % vs DEM ~16 %).
· ⇒ No SE material setting reproduces both the dip shape and the absolute value.
· The dip lives in the initial rigid-sphere packing geometry. A continuum cannot have it, regardless of material.
Capability division is a measured conclusion, not an assumption: DEM owns packing, MPM owns plastic shape.
Notes: "MPM 에 dip 이 없으면 MPM 이 틀린 것 아니냐"는 질문이 옵니다. 답: 표현 범위 밖이라는 뜻입니다. 연속체에는 "공"이 없습니다.

## Slide 9
Results and discussion
Bazzoun et al., J. Power Sources 661 (2026) 238682 · Holm, Electric Contacts (1967)
Battery Materials Lab.
8
■ Transport: a resistor network on voxels — validated by an independent paper
· Microstructure → 0.4 µm voxels (2.5 voxels across an SE particle); neighbouring same-phase voxels become resistors; solve ∇·(σ∇φ) = 0.
· Each contact neck carries a constriction resistance R = 1/(2σ·r_c) (Holm 1967); plastic contact area from Tabor.
· Three conductivities at once — ionic (SE) · electronic (AM + carbon) · thermal (three parallel paths)
· Coverage of AM by SE, verified against a model-independent geometric ground truth: direct contact 16 % / including plastic spreading 52 %.
★ External validation — the strongest evidence we have Bazzoun 2026 applied the same material (LPSCl + NCM811), the same DEM code, and the same resistor-network method, and validated it against measured EIS and COMSOL FEM: network ≈ FEM ≈ experiment, and 32–98× faster. ⇒ our methodology was validated by someone else, not by us.
Notes: COMSOL 로 하면 되지 않냐는 질문의 답이 여기 있습니다. 저항망 ≈ FEM ≈ 실험이 남의 논문으로 입증됐고, 우리는 32-98배 빠릅니다.

## Slide 10
Results and discussion
Bruggeman, Ann. Phys. 416 (1935) · Holm (1967) · Trevisanello, AEM 11 (2021) 2003400
Battery Materials Lab.
9
■ Closed-form transport laws — and the data independently picks the textbook exponents
σ_ion = σ_grain · Cronau(r_SE) · (ε_eff)^½ · CN² · coverage^½ · f_p³ · C(τ)
σ_e = (σ_S·NCM_S)^(1−p) (σ_P·NCM_P)^p · ε_AM⁴ · √A · (T/d)^β · …
Exponent | Locked value | Source | Corpus result
ε_AM^a (backbone) | a = 4 | Stauffer–Bruggeman | picks exactly 4 out of {2 … 8}
√A (constriction) | 0.5 | Holm 1967 | picks exactly 0.5 (symmetric loss)
NCM(r)^β (grain size) | β = 1.5 | Trevisanello 2021 | picks 1.5
(p(1−p))^a (bimodal) | a = 1 | symmetric mixing | within noise
· LOOCV σ_ion 0.975 (5 free parameters) · σ_e 0.953 — LOOCV = hide one case, learn from the rest, predict it; memorising cannot score.
· ★ The exponents were taken from the literature and held fixed — the scan below costs zero degrees of freedom, so this is validation, not fitting.
Notes: 여기서 강조할 것: 5개 지수를 우리가 맞춘 게 아니라 문헌에서 가져와 고정했고, 코퍼스가 그 값을 독립적으로 골라냈다는 것입니다.

## Slide 11
Results and discussion
Bruggeman, Ann. Phys. 416 (1935) 636
Battery Materials Lab.
10
■ Thermal transport has NO scaling law — and that is the result
· σ_ion rides one backbone (SE) and σ_e rides one backbone (AM). Heat instead travels three paths at once — AM-AM, AM-SE, SE-SE.
Chart: Which functional form can represent κ?
| A. pure power law | B. Bruggeman EMT | C. Ridge (14 features)
LOOCV | 0.59 | 0 | 0.9
· B (effective-medium theory) gives a negative baseline R² (−0.15 … −1.53) — shown as 0 in the chart.
· The 0.3 LOOCV gap between A and C is the quantitative proof that composite thermal transport is not a single-backbone scaling law.
· Every lever was exhausted — α sweep, cross terms, greedy over all 246 features, target transforms: max +0.017 = noise.
· ⇒ Ridge is the irreducible representation at this corpus size — a finding about the physics, not a modelling preference.
Notes: "왜 열만 회귀냐, 일관성이 없다"는 질문이 옵니다. 답: 그게 결과입니다. 단일 골격이 아니라서 원리적으로 스케일링이 안 됩니다.

## Slide 12
Results and discussion
Bard & Faulkner, Electrochemical Methods (2001) — Butler–Volmer
Battery Materials Lab.
11
■ Why a mixed-conducting additive helps — decomposed for the first time
· Same skeleton, same property table, same boundary conditions; only the additive differs (3.18 mAh/cm², 72.5 µm).
· σ_e +52.0 % · σ_ion +5.6 % · reaction interface area +18 % → total polarization at 1C: 46 → 41 mV.
Chart: Decomposition of the 4.7 mV polarization gap (mV)
| reaction area +18% | ionic σ +5.6% | electronic σ +52%
contribution to the 4.7 mV gap | 3.6 | 1 | 0.002
· reaction area → 3.6 mV (78 %)
· ionic σ → 1.0 mV (22 %)
· electronic σ → 0.002 mV (≈ 0 %)
· ★ At low rate the voltage gap is governed by reaction area, not by σ_e — σ_e is already 10⁴× better than σ_ion, so it is not the bottleneck.
· σ_e matters where the current is large: high rate and thick electrodes.
· This split is impossible experimentally — EIS and the discharge curve give only the sum.
Notes: "σ_e 를 52% 올렸는데 0.002 mV 라고?"라는 질문이 반드시 옵니다. 답: 직렬 저항에서는 작은 쪽이 지배합니다. 전자망은 이미 병목이 아닙니다.

## Slide 13
Results and discussion
σ_SDCP value is ASSUMED — swept, not asserted
Battery Materials Lab.
12
■ The additive relieves series resistance — it does not carry the current
· Swept the additive conductivity 15 → 1500 S/cm with the microstructure and ionic network held fixed.
Chart: Gain rises while the additive’s share of dissipation falls
| 15 | 50 | 150 | 250 | 1500
σ_e gain vs SBE (%) | 0.8 | 25.8 | 45.5 | 52 | 63.4
SDCP dissipation share (%) | 19.6 | 16.3 | 10 | 7.3 | 1.7
· ★ The gain grows (+0.8 → +63.4 %) while the additive’s share of dissipation falls (19.6 → 1.7 %).
· A phase that carried the current would show a rising share. The inversion is the signature of a phase that relieves a series resistance.
· ⇒ Practical consequence: the conclusion does not depend on knowing σ_SDCP. Even at the worst value (15 S/cm) the additive costs nothing (+0.8 %).
· Ionic conductivity and reaction area are unchanged across the sweep — the effect is isolated to the electronic channel.
We claim HOW the additive helps — a mechanism — not HOW MUCH. The mechanism survives the whole sweep.
Notes: σ_SDCP 250 은 측정값이 아니라 assumed 입니다. 그래서 값 하나로 결론을 내지 않고 5점을 스윕했고, 결론 두 가지가 모두 값에 안 걸립니다.

## Slide 14
Results and discussion
Bucci et al., J. Mater. Chem. A (2017) · Yun et al., Energy Storage Mater. (2023)
Battery Materials Lab.
13
■ What we do NOT know yet — two limits, quantified
(a) Cycle degradation is dominated by chemistry — contact loss is a lower bound of ~2 %
Piece | Physics | Share of fade | Anchor
contact–mechanical | shrinkage → contact opening (CZM) | ~2 % (lower bound) | mono 1.05× vs bimodal 1.51×
chemical CEI | diffusion-limited √N growth | ~98 % | Yun 2023 (this lab) R_ct 2.87× @100 cyc
OTHER | skeleton rearrangement · SE decomposition · Li side | dominant in coated cells | awaiting experiment
· The magnitude is anchored to an experimental endpoint; the shape (√N) is labelled ASSUMED — one endpoint cannot distinguish √N from linear. A tool decides it once ≥ 4 experimental points exist.
[Fig] contact-mechanical ~2 % vs chemical CEI ~98 % — three-way split of the fade
The magnitude is anchored to experiment; the shape stays labelled ASSUMED until four cycle points exist.
Notes: 열화의 98 % 가 화학이라는 것이 결론입니다. 접촉 2 % 는 반드시 "하한"이라고 말해야 합니다 — OTHER 가 모델 밖에 있습니다.

## Slide 15
Results and discussion
this work, Aug 2026 — rejection → mechanism → descriptor → grid check
Battery Materials Lab.
14
■ A rejected assumption, traced to its cause — and then to a one-number fix
· We indexed the SE stress response by phi = V_SE /(A*h - V_AM) ("how full is the SE’s own space") and assumed one curve would serve every electrode. Measured at matched loading rate, it does not: 2.96 - 3.83x at the same phi.
Chart: One geometric descriptor collapses the composition effect
| 501 | 620 | 745 | 916 | 1458
sigma at phi = 0.72 | 0.7001 | 0.5457 | 0.4921 | 0.4671 | 0.3743
· 1. Mechanism — von Mises caps only the shape-changing stress, not the pressure. One bed stops at 0.278 GPa (below the 0.30 yield) = still flowing into voids; the other reaches 1.012 GPa (3.4x yield) = pressurised, unable to reach the remaining voids.
· 2. The cause is composition, not thickness — five beds matched to +/-1.4 % in thickness, only the particle-size ratio varied, give 1.87x, perfectly monotonic in that ratio (by chance about 7e-5).
· 3. The fix — index by channel width instead: sigma proportional to d_h^-0.54, R2 = 0.935. A new electrode then needs only its d_h, not a new five-point curve.
· 4. Not a grid artefact — refining makes it stronger. Three grids (1.18 / 1.77 / 2.65 cells across the narrowest channel) give 1.70 -> 1.87 -> 2.03, monotonic. An unresolved constriction simply vanishes and lets material through, so coarse grids under-report the effect. Reported as a lower bound: |slope| >= 0.66.
Sensitivity scales with cells-per-channel: >= 3.5 cells moves only 4 % under a 2.25x refinement, 1.2 cells moves 24 % — a pre-run check we now apply to every bed.
Notes: Q: "전이가 기각됐으면 지금까지 결과가 다 틀린 것 아니냐" — 아닙니다. 기각된 것은 곡선을 다른 전극에 옮기는 것이고, 각 전극에서 직접 계산한 값은 무관합니다. 4번은 제 사전 예상이 부호부터 틀렸던 경우입니다 — 미해상이면 뻣뻣해질 줄 알았는데 실제로는 협착이 격자에서 사라져 오히려 무릅니다. Q: "그럼 지수 −0.66 이 참값이냐" — 아닙니다. 세 격자의 증분이 +0.170, +0.163 로 거의 안 줄어 겉보기 수렴차수가 0.10 입니다. 즉 아직 수렴 전이고, 하한으로만 보고합니다. 완전 해상하려면 n_grid ~900 이 필요한데 384 조차 35 GB 로 V100 을 넘습니다. Q: "그럼 기준곡선도 못 믿는 것 아니냐" — 아닙니다. 민감도는 채널당 셀 수의 함수이고, 기준곡선은 3.56~5.41 셀에서 쟀습니다. 그 밴드에서는 2.25배 정밀화에 4 % 만 움직입니다.

## Slide 16
Future plan
Battery Materials Lab.
15
■ Closing the last verification loop, then scaling to design
① Ready to run (code complete)
Item | Needs | Gives
PyBaMM matched-condition parity | one GPU day | defensible → bullet-proof
σ(φ, d_h) exponent at finer grid | n_grid 288 (~4 h) | converged value (now bounded: ¦slope¦ ≥ 0.54)
COMSOL hybrid export | bridge geometry | share results in COMSOL users’ language
② Awaiting anchors — we do not pretend to know
· LPSCl decomposition activation energy — confirmed absent from the literature ⇒ we do NOT multiply heat into degradation by Arrhenius.
· CEI √N shape confirmation (≥ 4 experimental points)
· measured σ_e of the additive · binding energy from DFT · i₀ split for single- vs poly-crystal
③ Machine learning — the differentiator is physics-derived features
· Now: design → σ triad surrogate (LOOCV 0.975 / 0.953 / 0.90) — seconds instead of hours.
· Next: cycle-life surrogate = 13 design + 15 physics features (σ triad · coverage · CN · τ · current focusing · reaction area) + cycle → R_int(N), retention.
· Then: closed design loop (symbolic regression + Bayesian optimisation → recommend the next composition to make).
· Materials side: MLIP (MACE / UMA) to resolve LPSCl disorder and produce DFT anchors — continuing from the April talk.
Experiments say "this composition is better". This pipeline says why, at which contact, and by how much.
Notes: 마지막 문장이 이 발표의 결론입니다.

## Slide 17
Appendix
A. technical backup · B. glossary & symbol conventions · C. anticipated questions

## Slide 18
Appendix A · Material parameters live on three levels
Sakuda et al., Sci. Rep. 3 (2013) 2261 · Cronau et al., ACS Energy Lett. 6 (2021) 3072
Battery Materials Lab.
16
■ The 18× softening is a proxy for missing mechanisms — never claimed as a material property
Level | Value | What it means
Real bulk LPSCl | E = 24 GPa (Young) B0 = 26.2 GPa (bulk, our DFT) | E from literature; the bulk modulus B0 is the quantity to compare against K, and comes from our own equation-of-state calculation
DEM effective | E_eff = 1.35 GPa | lumps rearrangement + grain-boundary sliding + micro-fracture that rigid spheres cannot do
MPM champion | E = 1.53 GPa, ν = 0.49 (K = 25.5, µ = 0.51 GPa) | softening confined to SHEAR. Bulk: our K 25.5 vs our DFT EOS B0 = 26.2 GPa (−2.8 %). Shear: µ 0.51 vs the real 8.1 GPa = ~16x softer. (Compare K to B0, never to E — different quantities.)
· Why it is not a free fit — three independent routes demand the same value:
· ① pure-SE contact overlap 11–12 % is reproduced (Cronau) ② an entirely different code and physics (MPM continuum) independently requires the same 18× ③ experimental porosity.
· Heckel compaction: R² 0.965 · yield pressure P_y = 138 MPa · σ_y,eff 46 MPa — 6.5× softer than the single crystal, which quantifies the granular softening.

## Slide 19
Appendix B · Glossary — terms as used in the field
full list with references: docs/seminar_20260806_glossary.md
Battery Materials Lab.
17
Term | In one line | Reference
DEM (discrete element method) | each particle is a rigid sphere; solve Newton | Cundall & Strack 1979
MPM (material point method) | continuum, carried on material points | Sulsky et al. 1994
Constriction resistance | extra resistance of a narrow contact neck R = 1/(2σa) | Holm 1967 · Maxwell 1873
Plastic contact area | A = F/H — larger than the elastic Hertz area | Tabor 1948
Percolation | is there a connected path end to end? | Stauffer & Aharony
Tortuosity τ | how far ions detour; σ_eff = σ_bulk·ε/τ (linear convention) | ⚠ state the convention
Coordination number CN | how many neighbours a particle touches | packing standard
Coverage | fraction of AM surface covered by SE | Hertz 16 % / Tabor 52 %
Overpotential η | the extra voltage needed to drive the reaction | Bard & Faulkner
CEI | resistive interphase that grows every cycle | Yun et al. 2023
⚠ Symbol collisions to state explicitly: φ = potential (V) vs volume fraction — use ε for fractions · σ = conductivity vs stress — always give units · τ convention (linear vs squared) differs between papers

## Slide 20
Appendix C · Anticipated questions
full set (40 Q&A): docs/seminar_20260806_script.md
Battery Materials Lab.
18
Question | First sentence of the answer
Isn’t this just fitted to experiment? | There is exactly one calibration point; everything after it is a prediction — and the two models never see each other.
Isn’t the 18× softening a free fit? | If it were free, three independent routes would not demand the same value.
σ_e up 52 % but only 0.002 mV? | Yes — in a series resistance the smaller one dominates, and σ_e was already 10⁴× better.
Where does σ_SDCP = 250 S/cm come from? | It is assumed, not measured — which is why we swept 15–1500 and claim only the mechanism.
If the transfer was rejected, is everything wrong? | No — what was rejected is moving one curve to another bed; quantities computed per bed are unaffected.
Why not just use COMSOL? | For σ and microstructure fields we can replace it — and an independent paper proved that; for liquid systems and full cells we cannot.
How does this help an experimentalist? | It decomposes why something works, points at what to fix, and screens candidates before they are made.
What is your weakest link? | Three: the external numerical parity run, the measured additive conductivity, and the experimental confirmation of the √N shape.