Table S2. Computational parameters for the DFT calculations of Li-adatom migration on the Li₃N(001) and LiC₆(0001) surfaces.

| Parameter | Li₃N(001) | LiC₆(0001) |
| --- | --- | --- |
| Code / functional | Quantum ESPRESSO 7.4.1 (pw.x) [1]; PBE [2] |  |
| Pseudopotentials | Li, N: ultrasoft | Li: ultrasoft; C: PAW |
| Cutoff (wavefunction / charge density) | 60 / 480 Ry |  |
| k-point mesh | 2 × 2 × 1 (Γ-centred) |  |
| Smearing | Marzari–Vanderbilt, 0.01 Ry [3] |  |
| Convergence (SCF / force) | 1 × 10⁻⁶ Ry / 1 × 10⁻³ Ry bohr⁻¹ |  |
| Slab model | α-Li₃N, 3 × 3; four Li₂N and three Li planes, Li₂N (N-exposed) termination; 135 atoms + 1 Li adatom | Stage-1 LiC₆, √3 × √3 R30°, 2 × 2 × 2; graphene-terminated; 108 atoms + 1 Li adatom |
| Cell / vacuum | a = b = 10.95 Å, c = 28.545 Å, γ = 120°; 15.7 Å vacuum | 15 Å vacuum |
| Fixed atoms | Bottom two Li₂N/Li bilayers | Bottom 50 % of the slab |
| Migration path | Constrained relaxationᵃ: adatom lateral (x, y) coordinates fixed; its height and all unconstrained atoms relaxed independently | CI-NEB [4] with the UMA-oc20 machine-learned potential [6] (7 images, IDPP initial path [5], 0.05 eV Å⁻¹) as implemented in ASE [7], then DFT single-point energies on those geometriesᵇ |
| Barrier definition | E(saddle-region configuration) − E(relaxed adsorption minimum) | E(highest-energy image) − E(initial adsorption minimum) |
| Migration barrier | 0.118 eV | 0.290 eV |

ᵃ Elastic-band calculations were unstable on the soft Li₃N(001) surface, so its barrier was evaluated from two independently converged constrained relaxations; the resulting 0.118 eV agrees with the 0.133 eV reported for the same surface in ref. [8].

ᵇ The LiC₆(0001) energies are DFT single points on machine-learned-potential geometries, which smooth the transition state; that barrier, and hence the ratio quoted in the main text, is a conservative lower bound.

References

[1] P. Giannozzi, S. Baroni, N. Bonini, M. Calandra, R. Car, C. Cavazzoni, D. Ceresoli, G. L. Chiarotti, M. Cococcioni, I. Dabo, A. Dal Corso, S. de Gironcoli, S. Fabris, G. Fratesi, R. Gebauer, U. Gerstmann, C. Gougoussis, A. Kokalj, M. Lazzeri, L. Martin-Samos, N. Marzari, F. Mauri, R. Mazzarello, S. Paolini, A. Pasquarello, L. Paulatto, C. Sbraccia, S. Scandolo, G. Sclauzero, A. P. Seitsonen, A. Smogunov, P. Umari, R. M. Wentzcovitch, QUANTUM ESPRESSO: a modular and open-source software project for quantum simulations of materials, J. Phys.: Condens. Matter 21 (2009) 395502. https://doi.org/10.1088/0953-8984/21/39/395502.

[2] J. P. Perdew, K. Burke, M. Ernzerhof, Generalized gradient approximation made simple, Phys. Rev. Lett. 77 (1996) 3865–3868. https://doi.org/10.1103/PhysRevLett.77.3865.

[3] N. Marzari, D. Vanderbilt, A. De Vita, M. C. Payne, Thermal contraction and disordering of the Al(110) surface, Phys. Rev. Lett. 82 (1999) 3296–3299. https://doi.org/10.1103/PhysRevLett.82.3296.

[4] G. Henkelman, B. P. Uberuaga, H. Jónsson, A climbing image nudged elastic band method for finding saddle points and minimum energy paths, J. Chem. Phys. 113 (2000) 9901–9904. https://doi.org/10.1063/1.1329672.

[5] S. Smidstrup, A. Pedersen, K. Stokbro, H. Jónsson, Improved initial guess for minimum energy path calculations, J. Chem. Phys. 140 (2014) 214106. https://doi.org/10.1063/1.4878664.

[6] B. M. Wood, M. Dzamba, X. Fu, M. Gao, M. Shuaibi, L. Barroso-Luque, K. Abdelmaqsoud, V. Gharakhanyan, J. R. Kitchin, D. S. Levine, K. Michel, A. Sriram, T. S. Cohen, A. Das, S. J. Sahoo, A. Rizvi, Z. W. Ulissi, C. L. Zitnick, UMA: A family of universal models for atoms, Adv. Neural Inf. Process. Syst. 38 (2025) 143528–143564. https://doi.org/10.52202/085713-4310.

[7] A. H. Larsen, J. J. Mortensen, J. Blomqvist, I. E. Castelli, R. Christensen, M. Dułak, J. Friis, M. N. Groves, B. Hammer, C. Hargus, E. D. Hermes, P. C. Jennings, P. B. Jensen, J. Kermode, J. R. Kitchin, E. L. Kolsbjerg, J. Kubal, K. Kaasbjerg, S. Lysgaard, J. B. Maronsson, T. Maxson, T. Olsen, L. Pastewka, A. Peterson, C. Rostgaard, J. Schiøtz, O. Schütt, M. Strange, K. S. Thygesen, T. Vegge, L. Vilhelmsen, M. Walter, Z. Zeng, K. W. Jacobsen, The atomic simulation environment—a Python library for working with atoms, J. Phys.: Condens. Matter 29 (2017) 273002. https://doi.org/10.1088/1361-648X/aa680e.

[8] M. S. Kim, Z. Zhang, J. Wang, S. T. Oyakhire, S. C. Kim, Z. Yu, Y. Chen, D. T. Boyle, Y. Ye, Z. Huang, W. Zhang, R. Xu, P. Sayavong, S. F. Bent, J. Qin, Z. Bao, Y. Cui, Revealing the multifunctions of Li3N in the suspension electrolyte for lithium metal batteries, ACS Nano 17 (2023) 3168–3180. https://doi.org/10.1021/acsnano.2c12470. (= ref. [54] of the main text)