2.5. Computational Methods

Density functional theory (DFT) calculations were performed with Quantum ESPRESSO and the Perdew–Burke–Ernzerhof generalized gradient approximation,[1–4] using SSSP efficiency pseudopotentials (ultrasoft for Li, B, P, S, and Cl; projector augmented-wave (PAW) for O) with kinetic energy cutoffs of 60 and 480 Ry for the wavefunctions and charge density.[5–7] Γ-centered Monkhorst–Pack k-point grids[8] and Marzari–Vanderbilt smearing[9] were used; the grids and convergence thresholds of each model are given in the Supporting Information.

Three structural models were constructed: LPSC1.6 (Li27P5S22Cl8), O-LPSC1.6 (Li27P5S21OCl8), and BO-LPSC1.6 (Li58P8B2S41O3Cl16; one B2O3 unit in a 1 × 1 × 2 LPSC1.6 supercell). The anion and Li+ arrangements and the dopant sites were selected with the Universal Model for Atoms (UMA) machine-learning interatomic potential,[10] and the O site of BO-LPSC1.6 was confirmed by DFT. For each model, the ionic positions were relaxed by DFT in isotropically scaled cells, and the energy–volume data were fitted to the third-order Birch–Murnaghan equation of state to obtain the equilibrium volume (V0) and bulk modulus (B0);[11] the structures relaxed at V0 were used in all subsequent analyses.

Li+ transport was simulated by UMA-based molecular dynamics (MD) in the NVT ensemble with a Langevin thermostat (time step 2 fs) at 600, 800, and 1000 K, using the Atomic Simulation Environment;[12] each run comprised 5 ps of equilibration and 200 ps of production, and at least three independent runs were performed for each model and temperature. The Li+ tracer diffusion coefficient (D) was obtained from linear fits of the mean square displacement (MSD) over 2–50 ps, the activation energy (Ea) from an Arrhenius fit of the run-averaged D, and the ionic conductivity from the Nernst–Einstein relation with a Haven ratio of 1 and D extrapolated to 273 K (Equations S1–S3 in the Supporting Information). Li+ migration pathways were mapped with a simplified bond valence site energy (BVSE) approach,[13] in which the site energy of a Li+ probe on a ~0.25 Å grid was approximated by the squared deviation of its bond valence sum from unity (Equation S4); the Li+ accessible volume fraction was defined as the fraction of grid points within 0.5 (valence units)2 of the global minimum.

The density of states (DOS) and projected DOS (PDOS) of BO-LPSC1.6 were calculated with the optimized tetrahedron method,[14] with energies referenced to the valence band maximum (VBM) of a fixed-occupation calculation. The electron localization function (ELF)[15] was evaluated at the bond midpoints and averaged over each bond type. Crystal orbital Hamilton population (COHP) analysis[16] was performed with LOBSTER 5.1.1 on PAW wavefunctions (charge spilling 1.19%),[17,18] and the integrated COHP (ICOHP) values up to the Fermi energy were averaged over each bond type. Bond lengths were averaged over first-shell pairs in the V0 structures.

References

1.	P. Giannozzi, S. Baroni, N. Bonini, M. Calandra, R. Car, C. Cavazzoni, D. Ceresoli, G. L. Chiarotti, M. Cococcioni, I. Dabo, A. Dal Corso, S. de Gironcoli, S. Fabris, G. Fratesi, R. Gebauer, U. Gerstmann, C. Gougoussis, A. Kokalj, M. Lazzeri, L. Martin-Samos, N. Marzari, F. Mauri, R. Mazzarello, S. Paolini, A. Pasquarello, L. Paulatto, C. Sbraccia, S. Scandolo, G. Sclauzero, A. P. Seitsonen, A. Smogunov, P. Umari, R. M. Wentzcovitch, J. Phys.: Condens. Matter 2009, 21, 395502.

2.	P. Giannozzi, O. Andreussi, T. Brumme, O. Bunau, M. Buongiorno Nardelli, M. Calandra, R. Car, C. Cavazzoni, D. Ceresoli, M. Cococcioni, N. Colonna, I. Carnimeo, A. Dal Corso, S. de Gironcoli, P. Delugas, R. A. DiStasio Jr., A. Ferretti, A. Floris, G. Fratesi, G. Fugallo, R. Gebauer, U. Gerstmann, F. Giustino, T. Gorni, J. Jia, M. Kawamura, H.-Y. Ko, A. Kokalj, E. Küçükbenli, M. Lazzeri, M. Marsili, N. Marzari, F. Mauri, N. L. Nguyen, H.-V. Nguyen, A. Otero-de-la-Roza, L. Paulatto, S. Poncé, D. Rocca, R. Sabatini, B. Santra, M. Schlipf, A. P. Seitsonen, A. Smogunov, I. Timrov, T. Thonhauser, P. Umari, N. Vast, X. Wu, S. Baroni, J. Phys.: Condens. Matter 2017, 29, 465901.

3.	P. Giannozzi, O. Baseggio, P. Bonfà, D. Brunato, R. Car, I. Carnimeo, C. Cavazzoni, S. de Gironcoli, P. Delugas, F. Ferrari Ruffino, A. Ferretti, N. Marzari, I. Timrov, A. Urru, S. Baroni, J. Chem. Phys. 2020, 152, 154105.

4.	J. P. Perdew, K. Burke, M. Ernzerhof, Phys. Rev. Lett. 1996, 77, 3865–3868.

5.	G. Prandini, A. Marrazzo, I. E. Castelli, N. Mounet, N. Marzari, npj Comput. Mater. 2018, 4, 72.

6.	K. F. Garrity, J. W. Bennett, K. M. Rabe, D. Vanderbilt, Comput. Mater. Sci. 2014, 81, 446–452.

7.	A. Dal Corso, Comput. Mater. Sci. 2014, 95, 337–350.

8.	H. J. Monkhorst, J. D. Pack, Phys. Rev. B 1976, 13, 5188–5192.

9.	N. Marzari, D. Vanderbilt, A. De Vita, M. C. Payne, Phys. Rev. Lett. 1999, 82, 3296–3299.

10.	B. M. Wood, M. Dzamba, X. Fu, M. Gao, M. Shuaibi, L. Barroso-Luque, K. Abdelmaqsoud, V. Gharakhanyan, J. R. Kitchin, D. S. Levine, K. Michel, A. Sriram, T. Cohen, A. Das, A. Rizvi, S. J. Sahoo, Z. W. Ulissi, C. L. Zitnick, arXiv 2025, arXiv:2506.23971.

11.	F. Birch, Phys. Rev. 1947, 71, 809–824.

12.	A. H. Larsen, J. J. Mortensen, J. Blomqvist, I. E. Castelli, R. Christensen, M. Dułak, J. Friis, M. N. Groves, B. Hammer, C. Hargus, E. D. Hermes, P. C. Jennings, P. B. Jensen, J. Kermode, J. R. Kitchin, E. L. Kolsbjerg, J. Kubal, K. Kaasbjerg, S. Lysgaard, J. B. Maronsson, T. Maxson, T. Olsen, L. Pastewka, A. Peterson, C. Rostgaard, J. Schiøtz, O. Schütt, M. Strange, K. S. Thygesen, T. Vegge, L. Vilhelmsen, M. Walter, Z. Zeng, K. W. Jacobsen, J. Phys.: Condens. Matter 2017, 29, 273002.

13.	R. P. Rao, S. Adams, Phys. Status Solidi A 2011, 208, 1804–1807.

14.	M. Kawamura, Y. Gohda, S. Tsuneyuki, Phys. Rev. B 2014, 89, 094515.

15.	A. D. Becke, K. E. Edgecombe, J. Chem. Phys. 1990, 92, 5397–5403.

16.	R. Dronskowski, P. E. Blöchl, J. Phys. Chem. 1993, 97, 8617–8624.

17.	S. Maintz, V. L. Deringer, A. L. Tchougréeff, R. Dronskowski, J. Comput. Chem. 2016, 37, 1030–1035.

18.	R. Nelson, C. Ertural, J. George, V. L. Deringer, G. Hautier, R. Dronskowski, J. Comput. Chem. 2020, 41, 1931–1940.